###### MAGNETIC POWDERS SYNTHESIED BY A SUBMERGED PULSED ARC

N. Parkanskya, G. Leitusb B. Alterkopa, Z. Barkayc,

Yu. Rosenbergc, and R.L.Boxmana

aElectrical Discharge and Plasma Laboratory, Tel Aviv University, POB 39040, Tel Aviv 69978, Israel
bDepartment of Chemical Research Support, Weizmann Institute of Science, Rehovot 76100, Israel

cWolfson Applied Materials Research Center, Tel Aviv University, POB 39040, Tel Aviv 69978, Israel

###### Carbon and Ni-C nanoparticles were synthesized using a pulsed arc between C and Ni electrode pairs submerged in pure ethanol. The arc was ignited by inter-electrode breakdown. 200 ml of ethanol was arc treated for 5 min with 1 s, 0.05 J pulses, at a repetition rate of ~1 kHz. The samples were examined by HRSEM, TEM, EDX and XRD, and their magnetic properties were studied in a SQUID magnetometer.

The powder produced using Ni electrodes consisted of carbon particles and nickel-carbon alloy particles. The latter were coated by carbon. The carbon concentration in the Ni alloy was approximately triple that of the maximum solid equilibrium solubility. 95% of produced particles had a diameter of less than 30 nm. It was found that the material was superparamagnetic in a wide temperature interval T>TB = 8 K. The material had a very narrow hysteresis loop Hc<8 Oe (i.e. it is a soft magnet) in the superparamagnetic state.

The powder  produced by using C electrodes showed at room temperature values of saturation magnetization Ms in the range of 2.0 to 3.8 emu/g, residual magnetization Mr=0.03-0.07 emu/g, and coercive force Hc = 15 - 35 Oe. The data suggests that the powder partially consisted of ferromagnetic carbon particles with a critical temperature greater than 300 K. Magnetic particles in solution were separated with a bio-ferrograph. It was found that the magnetically separated particles included chains of ~30-50 nm diam spheres, nanotubes and nano-rods with lengths of 50-250 nm and diameters of 20-30 nm. In contrast, the presumably unmagnetized particles which passed through the bio-ferrograph were 1 m and larger, and nano-particles of indefinite shape.