## Slide 1: Outline
Lecture 1 - Redox-Active Ligands: What Are They? How Do They Work? and How Might They Be Improved?
Lecture 2 - The Development of a Highly Active Manganese Hydrosilylation Catalyst
Lecture 3 - Hydrosilylation and Beyond: Expanding the Scope of Redox-Active Ligand Assisted Catalysts

## Slide 2: Homogeneous Transition Metal Catalysis
Hydrogenation (2001)
Dihydroxylation (2001)
Olefin Metathesis (2005)
Cross Coupling (2010)

## Slide 3: Homogeneous Transition Metal Catalysis
Hydrogenation (2001)
Dihydroxylation (2001)
Olefin Metathesis (2005)
Cross Coupling (2010)
Can First Row Transition Metals be Used Instead?

## Slide 4: Advantages
Cost Per Mole:
Based on Cheapest Available Starting Material Offered by Strem Chemicals (08/13)
First Row Metals Are:
- Three Orders of Magnitude Cheaper

## Slide 5: Advantages
Cost Per Mole:
Based on Cheapest Available Starting Material Offered by Strem Chemicals (08/13)
First Row Metals Are:
- Three Orders of Magnitude Cheaper
- Earth Abundant

## Slide 6: Advantages
Cost Per Mole:
Based on Cheapest Available Starting Material Offered by Strem Chemicals (08/13)
First Row Metals Are:
- Three Orders of Magnitude Cheaper
- Earth Abundant
- Significantly Less Toxic
RDAs: Mn (2.3 mg), Fe (8 mg)
5 ppm Limit for Precious Metals

## Slide 7: Mn Catalysis: The Road Less Traveled
Oxidation:
Zhang, W.; Loebach, J. L.; Wilson, S. R.; Jacobsen, E. N. J. Am. Chem. Soc. 1990, 112, 2801.

## Slide 8: Mn Catalysis: The Road Less Traveled
Oxidation:
Reduction:
Zhang, W.; Loebach, J. L.; Wilson, S. R.; Jacobsen, E. N. J. Am. Chem. Soc. 1990, 112, 2801.
Cavanaugh, M. D.; Gregg, B. T.; Cutler, A. R. Organometallics 1996, 15, 2764.
Pt Hydrosilylation Catalysts Currently Used for Coatings, Adhesives, and Cured Rubbers

## Slide 9: Catalyst Design Inspiration
Improved Mn Hydrosilylation Catalysts?

## Slide 10: Metallation of NPDI Ligands
Tufan Mukhopadhyay
- κ3-PDI Coord. Verified by XRD
- μeff = 6.0 μB
- High-Spin Mn(II)
- μeff = 6.3 μB
- High-Spin Mn(II)

## Slide 11: Chemical Chelate Activity
Tufan Mukhopadhyay
- Mn Center Remains Divalent
- Redox-Activity Leads to Deprotonation
- Observed with xs. K and COT (cat.)
- (Me2NPrPDI)MnCl2 Reduction Resulted in Decomposition
- μeff = 3.8 μB
- Intermediate-Spin Mn(II)

## Slide 12: Crystallographic Confirmation
Tufan Mukhopadhyay
Mn(1)-N(1) | 2.116(2)
Mn(1)-N(2) | 2.153(3)
Mn(1)-N(3) | 2.216(2)
N(1)-C(3) | 1.364(3)
C(3)-C(4) | 1.366(4)
C(3)-C(5) | 1.495(4)
N(1)-Mn(1)-N(1A) | 148.53(12)
N(2)-Mn(1)-N(3) | 126.54(5)
N(3)-Mn(1)-N(3A) | 106.91(11)

## Slide 13: (Ph2PPrPDI)MnCl2
Tufan Mukhopadhyay
- μeff = 6.1 μB
- High-Spin Mn(II)

## Slide 14: (Ph2PPrPDI)MnCl2
Tufan Mukhopadhyay
- μeff = 6.1 μB
- High-Spin Mn(II)
Mn(1)-Cl(1) | 2.3514(8)
Mn(1)-Cl(2) | 2.3748(8)
Mn(1)-N(1) | 2.300(2)
Mn(1)-N(2) | 2.196(2)
Mn(1)-N(3) | 2.338(2)
N(1)-Mn(1)-N(3) | 141.81(8)
Cl(1)-Mn(1)-Cl(2) | 112.13(3)
N(2)-Mn(1)-Cl(1) | 113.63(6)
N(2)-Mn(1)-Cl(2) | 133.16(7)
κ3-N,N,N-PDI Rather Than κ2-P,P-PDI Coordination

## Slide 15: Analyzing Chelate Reduction by XRD
Neutral
Radical Monoanion
Dianion
1.28 Å
Knijnenburg, Q.; Gambarotta, S.; Budzelaar, P. H. M. Dalton Trans. 2006, 5442.
1.32 Å
1.36 Å
1.50 Å
1.44 Å
1.40 Å
1.278(4) Å
1.493(4) Å
1.502(4) Å
1.282(3) Å
Tufan Mukhopadhyay

## Slide 16: Analyzing Chelate Reduction by XRD
Neutral
Radical Monoanion
Dianion
1.28 Å
Knijnenburg, Q.; Gambarotta, S.; Budzelaar, P. H. M. Dalton Trans. 2006, 5442.
1.32 Å
1.36 Å
1.50 Å
1.44 Å
1.40 Å
(Ph2PPrPDI)MnCl2: HS Mn(II), PDI0
1.278(4) Å
1.493(4) Å
1.502(4) Å
1.282(3) Å
Tufan Mukhopadhyay

## Slide 17: (Ph2PPrPDI)Mn Preparation
Tufan Mukhopadhyay
- Without COT, Reduction Takes 3.5 Days
- Formally Zerovalent, Deprotonation Not Observed
- For Pyridine vs. PR3 Substituents, It’s All About Covalency
- μeff = 2.2 μB (S = 1/2)

## Slide 18: (Ph2PPrPDI)Mn Characterization
Tufan Mukhopadhyay
1H NMR

## Slide 19: (Ph2PPrPDI)Mn Electronic Structure
Tufan Mukhopadhyay
Mn(1)-N(1) | 1.944(2)
Mn(1)-N(2) | 1.887(2)
Mn(1)-N(3) | 1.949(2)
Mn(1)-P(1) | 2.2697(8)
Mn(1)-P(2) | 2.2634(8)
N(1)-C(2) | 1.354(3)
C(2)-C(3) | 1.416(4)
C(7)-C(8) | 1.414(3)
N(3)-C(8) | 1.355(3)
N(1)-Mn(1)-N(3) | 157.54(9)
P(1)-Mn(1)-P(2) | 105.93(3)
N(2)-Mn (1)-P(1) | 130.90(6)
N(2)-Mn(1)-P(2) | 123.14(6)

## Slide 20: (Ph2PPrPDI)Mn Electronic Structure
Tufan Mukhopadhyay
Dianion
1.36 Å
1.40 Å
Mn(1)-N(1) | 1.944(2)
Mn(1)-N(2) | 1.887(2)
Mn(1)-N(3) | 1.949(2)
Mn(1)-P(1) | 2.2697(8)
Mn(1)-P(2) | 2.2634(8)
N(1)-C(2) | 1.354(3)
C(2)-C(3) | 1.416(4)
C(7)-C(8) | 1.414(3)
N(3)-C(8) | 1.355(3)
N(1)-Mn(1)-N(3) | 157.54(9)
P(1)-Mn(1)-P(2) | 105.93(3)
N(2)-Mn (1)-P(1) | 130.90(6)
N(2)-Mn(1)-P(2) | 123.14(6)

## Slide 21: (Ph2PPrPDI)Mn Electronic Structure
Tufan Mukhopadhyay
Electronic Structure:
Low-Spin Mn(II), PDI2-
Dianion
1.36 Å
1.40 Å
Mn(1)-N(1) | 1.944(2)
Mn(1)-N(2) | 1.887(2)
Mn(1)-N(3) | 1.949(2)
Mn(1)-P(1) | 2.2697(8)
Mn(1)-P(2) | 2.2634(8)
N(1)-C(2) | 1.354(3)
C(2)-C(3) | 1.416(4)
C(7)-C(8) | 1.414(3)
N(3)-C(8) | 1.355(3)
N(1)-Mn(1)-N(3) | 157.54(9)
P(1)-Mn(1)-P(2) | 105.93(3)
N(2)-Mn (1)-P(1) | 130.90(6)
N(2)-Mn(1)-P(2) | 123.14(6)
Confirmed by observation of an anisotropic 6-line EPR signal at 77K (SMn = 1/2)

## Slide 22: Hydrosilylation Activity
Tufan Mukhopadhyay
>99% Conversion
TOF = 1,485 h-1

## Slide 23: Other Silanes?
Tufan Mukhopadhyay
Silane | Product | % Conversion | TOF (h-1)
 |  | >99 | 1,485
 |  | 26 | 390
 | - | - | -

## Slide 24: Other Silanes?
Tufan Mukhopadhyay
Silane | Product | % Conversion | TOF (h-1)
 |  | 28 | 420
 |  | 5 | 75
 |  | 3 | 45
 | - | - | -

## Slide 25: Scope of Ketone Hydrosilylation
Tufan Mukhopadhyay
Substrate | Product (Ratio) | % Conv. | Time | TOF (h-1)
 | PhSiH(OCH(Me)(Ph))2 PhSi(OCH(Me)(Ph))3 (3:1) | >99 | 4 min | 1,485
 | PhSiH(OCH(Me)(Ar))2 PhSi(OCH(Me)(Ar))3 (5:1) | >99 | 25 min | 238
 | PhSiH(OCH(Me)(Ar))2 | >99 | 6 h | 17

## Slide 26: Scope of Ketone Hydrosilylation
Tufan Mukhopadhyay
Substrate | Product (Ratio) | % Conv. | Time | TOF (h-1)
 | PhSiH(OCH(Me)(Ar))2 PhSi(OCH(Me)(Ar))3 (7:1) | >99 | 4 h | 25
 | PhSiH(OCH(Me)(Ar))2 PhSi(OCH(Me)(Ar))3 (3:1) | >99 | 3.5 h | 28
 | PhSiH(OCH(CF3)(Ph))2 PhSi(OCH(CF3)(Ph))3 (2:1) | >99 | 12 h | 8

## Slide 27: Scope of Ketone Hydrosilylation
Tufan Mukhopadhyay
Substrate | Product (Ratio) | % Conv. | Time | TOF (h-1)
 | PhSiH(OCH(iPr)2)2 PhSiH2(OCH(iPr)2) (1:1) | >99 | 36 min | 165
 | PhSiH(OCH(Cy)2)2 PhSiH2(OCH(Cy)2) (3:1) | >99 | 24 h | 4
 | PhSiH(OCH(Me)(Ar))2 | 80 | 5 d | <1

## Slide 28: Scope of Ketone Hydrosilylation (0.1 mol %)
Tufan Mukhopadhyay
Substrate | Product (Ratio) | % Conv. | Time | TOF (h-1)
 | PhSiH(OCH(Me)(Ph))2 PhSi(OCH(Me)(Ph))3 (5:1) | >99 | 4 min | 14,850
 | PhSiH(OCy)2 | >99 | 4 min | 14,850
 | PhSiH(OCH(Me)(nBu))2 | >99 | 4 min | 14,850
Exothermic!

## Slide 29: Improving Atom-Efficiency
Tufan Mukhopadhyay
Substrate | Product (Ratio) | % Conv. | Time | TOF (h-1)
 | PhSi(OCy)3 | >99 | 4 h | 74
 | PhSi(OCH(Me)(Ph))3 | >99 | 6.5 h | 46
 | PhSiH(OCH(Me)(nBu))2 PhSi(OCH(Me)(nBu))3 (3:1) | 74 | 24 h | 9

## Slide 30: Only the Beginning...
Tufan Mukhopadhyay
>99% Conversion

## Slide 31: Only the Beginning...
Tufan Mukhopadhyay
Ester Dihydrosilylation by way of Reductive C-O Bond Cleavage
>99% Conversion

## Slide 32: Only the Beginning...
Tufan Mukhopadhyay
- >99% Conversion
- TOF = 18 h-1 (vs. EtOAc)
- Selective for PhSi(OEt)3
>99% Conversion

## Slide 33: Other Esters
Tufan Mukhopadhyay
Substrate | Product (Ratio) | % Conv. | Time
 | PhSi(OEt)3 PhSiH(OiPr)2 PhSi(OiPr)3 PhSiH(OEt)2 (2:1.5:1:1) | >99 | 3 d (80 °C)
 | PhSi(OPh)3 PhSi(OEt)3 PhSi(OEt)2(OPh) (1.25:1.25:1) | 95 | 10 d (25 °C)
 | PhSiH(OtBu)2 PhSiH(OEt)(OtBu) PhSi(OEt)3 (1.25:1.25:1) | 85 | 10 d (80 °C)
Consistent with Previously Reported Acyl C-O Bond Cleavage Preferences

## Slide 34: A Curious Observation
Tufan Mukhopadhyay
1H NMR: -2.98 (t, JPH = 112.5 Hz, 1H, Mn-H)

## Slide 35: A Curious Observation
Tufan Mukhopadhyay
1H NMR: -2.98 (t, JPH = 112.5 Hz, 1H, Mn-H)
Active Catalyst?
Are Activities (TOFs) Really 10x-1,000x Higher?

## Slide 36: Alternate Preparation
Tufan Mukhopadhyay
- Diamagnetic
- 31P NMR: 69.20 (s)
- Converts to (Ph2PPrPDI)Mn After Days
1H NMR

## Slide 37: Alternate Preparation
Tufan Mukhopadhyay
- Diamagnetic
- 31P NMR: 69.20 (s)
- Converts to (Ph2PPrPDI)Mn After Days
1H NMR
Low-Spin Mn(I)?

## Slide 38: (Ph2PPrPDI)MnH Electronic Structure
Tufan Mukhopadhyay
Mn(1)-H | 1.57(3)
Mn(1)-N(2) | 1.945(2)
Mn(1)-N(1) | 1.860(2)
Mn(1)-N(3) | 1.947(2)
Mn(1)-P(1) | 2.2067(8)
Mn(1)-P(2) | 2.2158(7)
N(2)-C(6) | 1.351(3)
C(6)-C(5) | 1.424(4)
C(1)-C(23) | 1.418(3)
N(3)-C(23) | 1.342(3)
N(1)-Mn(1)-H | 175.0(11)
N(2)-Mn(1)-N(3) | 158.81(9)
P(1)-Mn(1)-P(2) | 123.85(3)
N(1)-Mn(1)-P(1) | 114.01(6)
N(1)-Mn(1)-P(2) | 122.14(6)

## Slide 39: (Ph2PPrPDI)MnH Electronic Structure
Tufan Mukhopadhyay
Mn(1)-N(1) | 1.944(2)
Mn(1)-N(2) | 1.887(2)
Mn(1)-N(3) | 1.949(2)
Mn(1)-P(1) | 2.2697(8)
Mn(1)-P(2) | 2.2634(8)
N(1)-C(16) | 1.354(3)
C(16)-C(18) | 1.416(4)
C(19)-C(23) | 1.414(3)
N(3)-C(23) | 1.355(3)
N(1)-Mn(1)-N(3) | 157.54(9)
P(1)-Mn(1)-P(2) | 105.93(3)
N(2)-Mn (1)-P(1) | 130.90(6)
N(2)-Mn(1)-P(2) | 123.14(6)
(Ph2PPrPDI)MnH
(Ph2PPrPDI)Mn
Mn(1)-H | 1.57(3)
Mn(1)-N(2) | 1.945(2)
Mn(1)-N(1) | 1.860(2)
Mn(1)-N(3) | 1.947(2)
Mn(1)-P(1) | 2.2067(8)
Mn(1)-P(2) | 2.2158(7)
N(2)-C(6) | 1.351(3)
C(6)-C(5) | 1.424(4)
C(1)-C(23) | 1.418(3)
N(3)-C(23) | 1.342(3)
N(1)-Mn(1)-H | 175.0(11)
N(2)-Mn(1)-N(3) | 158.81(9)
P(1)-Mn(1)-P(2) | 123.85(3)
N(1)-Mn(1)-P(1) | 114.01(6)
N(1)-Mn(1)-P(2) | 122.14(6)

## Slide 40: (Ph2PPrPDI)MnH Electronic Structure
Tufan Mukhopadhyay
(Ph2PPrPDI)MnH
Electronic Structure: Low-Spin Mn(III), PDI2-
Mn(1)-H | 1.57(3)
Mn(1)-N(2) | 1.945(2)
Mn(1)-N(1) | 1.860(2)
Mn(1)-N(3) | 1.947(2)
Mn(1)-P(1) | 2.2067(8)
Mn(1)-P(2) | 2.2158(7)
N(2)-C(6) | 1.351(3)
C(6)-C(5) | 1.424(4)
C(1)-C(23) | 1.418(3)
N(3)-C(23) | 1.342(3)
N(1)-Mn(1)-H | 175.0(11)
N(2)-Mn(1)-N(3) | 158.81(9)
P(1)-Mn(1)-P(2) | 123.85(3)
N(1)-Mn(1)-P(1) | 114.01(6)
N(1)-Mn(1)-P(2) | 122.14(6)

## Slide 41: Activity Comparison
Tufan Mukhopadhyay
Catalyst | Substrate | % Conv. | Time | TOF (h-1)
(Ph2PPrPDI)Mn |  | >99 | 4 min | 14,850
(Ph2PPrPDI)MnH |  | 87 | 4 min | 13,050
(Ph2PPrPDI)Mn |  | >99 | 4 min | 14,850
(Ph2PPrPDI)MnH |  | 80 | 4 min | 12,000

## Slide 42: Activity Comparison
Tufan Mukhopadhyay
Catalyst | % Conv. | Time | TOF (h-1)
(Ph2PPrPDI)Mn | >99 | 5.5 h | 18
(Ph2PPrPDI)MnH | >99 | 7 h | 14

## Slide 43: Mn-H Ketone Reduction Mechanism
Tufan Mukhopadhyay
Mn(III), PDI2- Maintained Throughout Transformation

## Slide 44: Radical Ketone Reduction Mechanism
Tufan Mukhopadhyay
Are Both Pathways Operative?

## Slide 45: Mn-H Ester Reduction Mechanism
Tufan Mukhopadhyay
Mn(III), PDI2- Maintained Throughout Transformation

## Slide 46: Mn-H Ester Reduction Mechanism
Tufan Mukhopadhyay
Mn(III), PDI2- Maintained Throughout Transformation

## Slide 47: Radical Ester Reduction Mechanism
Tufan Mukhopadhyay
Are Both Pathways Operative?

## Slide 48: Radical Ester Reduction Mechanism
Tufan Mukhopadhyay
Are Both Pathways Operative?

## Slide 49: A Revealing Experiment
Tufan Mukhopadhyay
‘Insertion’ of ketone into Mn-H is very slow! Not part of the catalytic cycle.
Bright Blue

## Slide 50: Summary
Lecture 2 - The Development of a Highly Active Manganese Hydrosilylation Catalyst
A formally zerovalent (PDI)Mn precatalyst was prepared

## Slide 51: Summary
Lecture 2 - The Development of a Highly Active Manganese Hydrosilylation Catalyst
A formally zerovalent (PDI)Mn precatalyst was prepared
This complex is highly active for the hydrosilylation of ketones

## Slide 52: Summary
Lecture 2 - The Development of a Highly Active Manganese Hydrosilylation Catalyst
A formally zerovalent (PDI)Mn precatalyst was prepared
This complex is highly active for the hydrosilylation of ketones
The reductive acyl C-O cleavage of esters has been observed