EXPERIMENTAL STUDY OF THE ISOCHORIC HEAT CAPACITY OF THE IONIC LIQUID ([C6mim][NTf2])

Polikhronidi N.G., Batyrova R.G., Abdulagatov I.M.

Institute of Physics of the Dagestan Scientific Center of the Rassian Academy of    Sciences, Russia, 367005, Makhachkala, Yaragskogo Str., 94.

E-mail: polikhronidi@rambler.ru

At conditions for one-phase liquid and for two-phase liquid + vapor equilibrium, isochoric heat capacities () and densities () were measured for ionic liquid (IL) 1-hexyl-3-methylimidazolium bis[(trifluoromethyl)sulfonyl] imide, often abbreviated [C6mim][NTf2]. Measurement were intensified near the liquid-gas phase transition curve in order to closely observe the changes. The measurements have been made over the temperature range from (330 to 480) K and pressures up to 20 MPa using a high-temperature, high-pressure, nearly constant-volume adiabatic calorimeter. Measurements were performed along 9 liquid isochores in the range between 1218 kg(m-3 and 1279 kg(m-3. The values of temperature at the liquid-gas phase transition curve for each measured isochore (phase transition parameters, ) were obtained by analysis of the quasistatic thermograms (reading of PRT, T-plot) and barograms (readings of the pressure transducer, P -plot). The combined expanded uncertainty of the density,, and isochoric heat capacity, , measurements at the 95 % confidence level with a coverage factor of k = 2 is estimated to be 0.06 % and 2.0 %, respectively. The combined expanded uncertainty of the phase-transition temperature is 0.02 K. One- () and two-phase () liquid isochoric heat capacities at saturation and saturation liquid densities () of IL ([C6mim][NTf2]) have been measured.

The measured values of saturated caloric () and saturated thermal () properties were used to calculate derived thermodynamic properties such as (,, W, ,) of [C6mim][NTf2] at saturated liquid conditions. The second temperature derivatives of the vapor pressure  and the chemical potential  at liquid + vapor conditions, and the second temperature derivative of pressure  at compressed liquid conditions were also calculated directly from the measured one- and two-phase isochoric heat capacity data. Values of  and   derived from calorimetric measurements were compared with the values calculated from vapor-pressure equations and from an IUPAC reference equation of state.

This work was supported by the Grant of RFBR NHK 13-08-00114/13.