THERMODYNAMICS FOR POLYKETONES SERIES IN THE INTERVAL FROM Т  0 TO 550 K

N.N. Smirnova, L.V. Nikishenkova, G.P. Belov

Chemistry Institute, Nizhny Novgorod State University, Russia, 603950,
Nizhny Novgorod Gagarin Pr. 23/5, smirnova@ichem.unn.ru

The alternating copolymers of monoxide carbon with the alicyclic and cyclic olefins, dienes, styrene and their derivatives are new class of functional macromolecules with potential valuables properties: thermoplasticity, shock resistance, high chemical stability and thermostability, nice adhesive behavior, lightness to skinning and high orientation fibers. It is obvious that the study of the thermodynamic properties and the thermodynamic parameters of their synthesis as well as the detection of the dependences of the thermodynamic characteristics on the structure and composition are necessary for the thermophysical calculations and optimization of the new compound synthesis processes.

In the present work by precision adiabatic vacuum and high-precision dynamic calorimetry the temperature dependences of heat capacity  = f(T), temperatures and enthalpies of physical transitions for series of the polyketones and the initial substances were studied in the range from 6 to (450550) K with the error of 0.5%. In an isothermal calorimeter with a static bomb the energies of combustion of the above substances were estimated with an error of ca. 0.02%. The experimental data were used to determinate the parameters of devitrification and the glassy state as well as the thermodynamic characteristics of melting and to calculate the standard thermodynamic functions (Т), [],  and [] for the range from T  0 to (450550) K; the standard thermochemical parameters of formation ,  and  of polyketones in a completely crystalline and amorphous states at T = 298.15 K were evaluated. The thermodynamic parameters of the polyketones synthesis in the range from 0 to (450550) were determined.

The dependences in change of standard thermodynamic properties for polyketones as thermodynamic parameters of their synthesis on the structure and composition, molecular weight, physical states and temperatures over range from Т  0 K to (340510) K are established. The obtained dependences allow to prediction of the thermodynamic properties and the thermodynamic synthesis parameters of the polyketones that are not studied yet by now.