DEFINITION of DEGREE OF CRYSTALLIZATION of the SPECIES AT EQUILIBRIUM CRYSTALLIZATION FROM the saturated SOLUTION

Aleksandrov V.D., Sobolev A.J.

Donbass national academy of civil engineering and architecture

Ukraine, 86123, Donetsk region, Makeyevka – 23, Derzhavin's street, 2 trashover@ukr.net

It is offered a method of definition of degree crystallization at equilibrium crystallization from the saturated solution. Experiment consists of 2 parts: graduation of the air thermostat in the furnace and getting thermograms of crystallization of a solution under the same conditions as furnace graduation (speed of heating, the maximum temperature). On an experimental curve 1 cooling of the furnace approximates by curve T(τ)= =Ae-Bτ+C. In the specimen on a section ad during τ1≤τ≤τn heat released due to process of equilibrium crystallization. Value of this heat is proportional to the area limited by lines ad, de and ae, i.e =κ  (1), where TL – temperature of crystallization of a solution, κ – an installation constant. At any moment of time τi value of heat is equal to the same integral with the top limit τi: =κ (2). Calculating the relation η(τ)=Qi/Q, we will receive degree of crystallization of the sample at any moment of time τ. By writing the Avrami-Kolmogorov's equation for two various moments of time τ1 and τ2 and founding a difference of these equations, it is possible to define index n= (3). By potentiating Avrami-Kolmogorov's equation we receiving expression for the constant of crystallization	Z(τ)= (4). Thus by means of thermograms it can be calculated: degree of crystallization at any moment τ; an indicator of the form of germs n; a constant of crystallization Z.

# Text boxes

e

d

c

2

1

τn

τi

τ1

T

a

b

Pic.1 Curves of cooling of the furnace (1) and specimen (2).

τ

TL