The melting enthalpy calculation and experimental determination of two- and three-component saline eutectic mixture

Garkushin I.K., Dvoryanova E.M., Aphanasieva O.U.

Samara state technical university, Russia, 443100, Samara, Molodogvardeiskaya st, 244. E-mail: baschem@samgtu.ru

Experimental determination specific melting enthalpy of eutectic mixture carried out on a setup DSC-D [1]. The experimental and design data account entropy of mixing (the design specific melting enthalpy is given by formulas 1 and 2) presented in table 1.

(Sе = x(S1 + (1-x)(S2 							(1)

;    		(2)

x is mass part compound of mix; (Sе, (S1, (S2 the specific melting entropy of eutectic and 1, 2 components; (Hе, (Н1, (Н2 the specific melting enthalpy of eutectic and 1, 2 components.

Table 1

The experimental and design specific melting enthalpy of eutectic mixture data

| Composition, mass % | (Нd | (Нe | ratio error, % |
| --- | --- | --- | --- |
| 48 % LiF + 52 % NaF | 716 | 711 | 0,8 |
| 31 % LiF + 69 % KF | 456 | 461 | 1,0 |
| 40 % LiF + 60 % MgF2 | 816 | 857 | 4,8 |
| 33 % NaF + 67 % KF | 497 | 517 | 3,9 |
| 67 % NaF + 33 % MgF2 | 694 | 628 | 10,5 |
| 33 % LiF +50 % NaF + 17 % MgF2 | 722 | 625 | 15,5 |
| 35 % LiF + 38 % NaF + 27 CaF2 | 557 | 528 | 11,3 |

The results given in table 1 show that ratio error is too little, therefore this method can be applied for approximate estimator of specific melting enthalpy.

References

1. Moshchenskiy U.V., Trunin A.S., Kosminin A.S. The thermal analysis system to calorimetric investigations. Scientific publication. Samara st. techn. un. Samara, 1999. P. 64.