THERMAL CAPACITY OF TRIPLE CHROMITE LaLiCaCr2O6

IN THE RANGE  298,15-673К

B.К. Кasenov, А.А.Mazhit, Sh.B. Kasenova, S.Zh. Davrenbekov,

Zh.I. Sagintaeva

JSC «Research-and-Production Center «Phytochemistry»

4 Gazaliev str., Karagamda, Kazakhstan, 100009

E-mail: phytoinform@nursat.kz

Rare earth metal chromites are known to possess a unique combination of electric, magnetic, thermal, optical and other properties and minor additions of alkaline earth metals to them enhance their electrical conductivity [1]. It should be noted that so far there are no data on thermodynamic properties of double or triple rare earth metal chromites, alkaline and alkali-earth metals.

We were the first to synthesize the triple chromite LaLiCaCr2O6 from respective carbonite oxides of metals and its formation was verified by X-ray analysis. This paper discusses the results of calorimetric studies on thermal capacity of the stated chromite performed on IT-C-400 apparatus in the range 298,15-673К. The chromite in question was found to undergo the second kind phase transition at 448К within the stated temperature range and with the account of  Тпр its C°p~f(T) dependence is described with the following equations  [J/(mol·К]:

= -(353 ± 21) + (1570 ± 92 ) ·10-3Т + (69,5  ±  4,1)·105Т-2  ,          (1)

= - (156 ± 9) + (205 ± 12) ·10-3Т + (901,4 ± 53,0)·105Т-2    ,          (2)

=  (1083 ± 64) - (654 ± 38) ·10-3Т – (1552,3 ± 91,3)·105Т-2 .        (3)

Reference

[1] Barykin B.I., Reznikova Е.D., Popil’skaya R.Ya. et al. Electro- & thermal conductivity of ceramics based on alloyed ittrium chromite // Thermophysics  of high temperatures. 1982. V.20. No.2. P.384-386.