THERMAL CAPACITY OF MANGANITES LaMeIMeIIMn2O6

(MeI-Li, Na, K, Rb; MeII-Mg, Ca, Ba) in the range 298,15-673 К

Zh.S. Bekturganov

JSC «Research-and-Production Center «Phytochemistry»

4 Gazaliev str., Karagamda, Kazakhstan, 100009

Е-mail: phytoinform@nursat.kz

Discovery of giant negative magnetoresistance in manganites like La1-x(Ca, Ba)xMnO3 in 1993-1994 laid the foundation for intense researches to find and studies of physical and chemical properties in similar. In this regard, we were the first to synthesize a series of triple manganites with the composition LaMeIMeIIMn2O6 (MeI-alkaline; MeII-alkali earth metals). This paper generalizes the results of our calorimetric studies to find С0р(f (Т) dependence on IT-C-400 apparatus (Table).

| Manganite | Equation coefficients С0р=a+в(T+c(T-2, J/mol(К | (Т, К |
| --- | --- | --- |
|  | а | в 10-3 | с 105 |  |
| LaLiMgMn2O6 | 204(9 | 262(12 | 11,3(0,5 | 298,15-673 |
| LaLiSrMn2O6 | 193(7 | 272(11 | 24,7(0,9 | 298,15-673 |
| LaLiBaMn2O6 | 335(18 | 149(8 | 94,2(5,0 | 298,15-673 |
| LaNaMgMn2O6 | 209(10 | 270(13 | 8,5(0,4 | 298,15-673 |
| LaNaCaMn2O6 | 126(6 | 325(15 | 5,6(0,3 | 298,15-673 |
| LaNaBaMn2O6 | 429(38 | 106(9 | 125,6(11,0 | 298,15-673 |
| LaKMgMn2O6 | 237(11 | 236(11 | 6,8(0,3 | 298,15-673 |
| LaKCaMn2O6 | 395(17 | 4(0,2 | 133,0(6,0 | 298,15-348 |
|  | 619(27 | -(1020(44) | - | 348-373 |
|  | -(75(3) | 733(31 | 5,8(0,2 | 373-673 |
| LaKSrMn2O6 | 211(18 | 269(23 | 14(1 | 298,15(573 |
|  | 1137(111 | -(1340(11) | - | 573-673 |
| LaRbMgMn2O6 | 267(12 | 284(12 | 36(2 | 298,15-673 |

Tabulated data show that LaKCaMn2O6 at 348 К and LaKSrMn2O6 at  573 К undergo (-type second kind  phase transition.