CRYSTALLIZATION OF OXIDIZED ISOTACTIC POLYPROPYLENE (PP)

Yu.V. Solovova, L.S. Shibryaeva

Russian Acad. Sci., Emanuel Inst. of biochemical physics, 119991 Moscow, Kosygina 4

yuli.m@inbox.ru (Yu.V. Solovova), shibr@pochtamt.ru (L.S. Shibryaeva)

It is well-known, that the noncrystallizing parts of macromolecules govern, first, diffusion of crystallizing chains to the crystallite surfaces; second, the orientational extension of crystallizing macromolecules; and, third, packing of macromolecules on nucleus surfaces, thus predeterming the crystallite growth. Therefore, factors such as the structure of through-pass macromolecules in a polymer and the content of loops, chain ends, and entanglements between macromolecules, substantially influence the structure of the crystallites being formed. Accordingly, it may be expected that the degradation, structuring, and a change in the chemical composition of through-pass chains in the oxidized polymer (these processes are caused by the thermal oxidation of the polymer and predetermined changes in the conformation, free volume, and segmental mobility of polymer chains) affect thermodynamic parameters of crystallization. The general character of these effects depends on the mechanism of oxidation and structural rearrangements accompanying the process. In other words, we may a priori state that the formation of crystallites in oxidized samples, as well as the thermodynamic and kinetic parameters of crystallization, will vary depending on structural rearrangements caused by the thermal oxidation.

The kinetics of isothermal crystallization of PP samples was investigated by differential scanning calorimetry. The influence of oxidation on the thermodynamic parameters of PP crystallization was estimated using the temperature dependence of the spherulite growth rate, Williams-Landel-Ferry equation and half-time of crystallization parameter t1/2. The value of energy barrier of nucleation W determined for PP samples reveal the effect of oxidation on the nucleation energy of PP. When passing from virgin to the oxidized PP samples, W increases, the higher the concentration of carbonyl groups accumulated in polymer chains, the more pronounced this effect.

The activation energy of crystallization E (which consists of free activation energy of diffusion of crystallizing element through phases boundary to front surface of crystalline and free energy of crystallization during formation of critical nucleus on the crystallization temperature) was calculated using the Arrenius equation and t1/2. It was founded, that the values of E for the virgin PP samples are lower than for oxidized PP. Increase of value of E is probably connected with a decline in the segmental mobility of functionalized through-pass chains or the strengthening of intermolecular interaction of oxidized macromolecules.