THERMODYNAMIC ESTIMATION OF REACTIONS OF OXIDIZED molybdenic products DISSOLUTION

## L.M. Karimova

Chemical-metallurgical Institute named after Z.H.Abishev, KZ, E-mail:lutsia.08@mail.ru

For an estimation of an dissolution opportunity of molybdenum from oxidized molybdenic promproduct with simultaneous use MgO and Na2CO3 calculations of their thermodynamic potentials are fulfild.

Under our assumptions, process of dissolution can proceed on reactions:

2MoO3+2MgO+2Na2CO3+H2O→MgMoO4+Na2MoO4+MgCO3+2NaOH+CO2,    (1)

2MoO3+2MgO+Na2CO3+H2O → MgMoO4+Na2MoO4+Mg(OH)2+ CO2,               (2)

2CuMoO4+MgO+Na2CO3+2H2O → Na2MoO4+MgMoO4+2Cu(OH)2+CO2,          (3)

2Fe2(MoO4)3+5MgO+Na2CO3+6H2O→Na2MoO4+5MgMoO4+4Fe(OH)3+CO2.      (4)

Received values , ,  and Кр of its reactions are resulted  in the table. On a method [1] calculations  and Кр per atom of molybdenum are lead. As show results of calculations, values  of reactions decrease from (1) to (3), so in turn, , the constant of speed increases probably.

The table-results of thermodynamic calculations of reactions (1 - 4)

| Number of reaction | ΔS0298, J/mole·K | -ΔH0298, kJ/mole | -ΔG0298, kJ/mole | lnKр | -ΔG0298, to [1] kJ/mole | lnKр, to [1] |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | -118,16 | 134,180 | 99,360 | 40,1037 | 49,68 | 20,05 |
| 2 | -81,814 | 153,495 | 129,110 | 52,1115 | 64,55 | 26,05 |
| 3 | 155,718 | 500,036 | 546,440 | 220,554 | 273,22 | 110,27 |
| 4 | 742,116 | 1445,81 | 1634,269 | 659,625 | 272,37 | 109,93 |

# literature

[1] H.K.Ospanov. Physical and chemical bases of selective dissolution of minerals.-М.: Bowels, 1993. 17-39.