MATHEMATICAL MODELING OF EXTRACTION ISOTHERMS OF MINERAL ACIDS WITH MIXTURES OF DI-(2-ETHYLHEXYL) PHOSPHORIC ACID AND QUATERNARY AMMONIUM SALTS

K.A. Slavinskiy, S.I. Stepanov

D. I. Mendeleyev University of Chemical Technology of Russia

Russian Federation, Moscow, Miusskaya sq., 9, e-mail: k.slavinskiy@mail.ru

There is an on-going demand for software suitable for analysis of experimental data obtained from investigation of equilibrium of extraction processes. We have developed "user friendly" software EXTREQ-2 [1] for mathematical modeling of extraction isotherms in multicomponent systems. Extraction equilibria of hydrochloric and nitric and sulfuric acids with mixtures of di-(2-ethylhexyl) phosphoric acid (D2EHPA) and methyl-three-alkyl-ammonium (MTAA) salts in toluene was investigated using software EXTREQ-2. The results of modeling of these extraction systems presented in table 1. Deviation of modeling curve from experimental data estimated by three criterions: relative error (R), and minimum mean square error (SSE), and residual dispersion (δR2).

Table 1. Mathematical modeling of extraction isotherms of mineral acids with mixtures di-(2-ethylhexyl) phosphoric acid and methyl-three-alkyl-ammonium salts

| Composition of organic phase | ln(KT) | H1 | R,% | SSE | δR2 |
| --- | --- | --- | --- | --- | --- |
| Extraction of HCl with 0.55 mol/L D2EHPA and 0.55 mol/L MTAA chloride |
| (RO)2P(O)O(R4N)∙HCl | 5.46 | 9.77 | 1.69 | 8.03×10-3 | 6.69×10-4 |
| (RO)2P(O)OH∙HCl | 0.88 | 7.86 |  |  |  |
| (R4N)Cl∙HCl | -3.63 | 4.69 |  |  |  |
| HCl | -3.54 | 11.76 |  |  |  |
| Extraction of HNO3 with 0.57 mol/L D2EHPA and 0.57 mol/L MTAA nitrate |
| (RO)2P(O)O(R4N)∙HNO3 | 4.91 | -3.83 | 2.26 | 1.35×10-2 | 1.04×10-3 |
| (RO)2P(O)O(R4N)∙NO3- | 3.08 | -0.53 |  |  |  |
| HNO3 | -2.37 | 5.99 |  |  |  |
| Extraction of H2SO4 with 0.53 mol/L D2EHPA and 0.53 mol/L MTAA sulphate |
| (RO)2P(O)O(R4N)∙H2SO4 | -1.77 | -4.06 | 2.41 | 7.78×10-3 | 7.07×10-4 |
| (RO)2P(O)O(R4N)∙HSO4- | 2.44 | 6.49 |  |  |  |
| H2SO4 | 0.08 | 7.40 |  |  |  |

The thermodynamic constants of extraction (KT) and parameters of hydratation (H1) for each of investigation systems were calculated and confirmed by independent physical chemistry methods of analyses.

REFERENCES

[1].	S.I. Stepanov, K.A. Slavinskiy. J. Chem. Tech. 10 (2006) 40-43 (in Russian)