ТЕРМОДИНАМИЧЕСКИЕ СВОЙСТВА БОРОГИДРИТОВ ЛАНТАНИДОВ

Б.А.Гафуров(1), У.М. Мирсаидов(2), М.С. Исломова(3), А.Б. Бадалов(3).

1) Кургантюбинский университет, Кургантюбе, Таджикистан.

2) Агентство по ядерной и радиационной безопасности АН Республики Таджикистан.

3) Таджикский технический университет, Душанбе, Таджикистан.

E-mail:badalovab@mail.ru

Сольватированные борогидриды лантанидов -  ЗТГФ (ТГФ-тетрагидрофуран) синтезированы обменной реакцией между хлоридами (лантанидов) и в среде ТГФ. Исследовано термическое разложение несольватированных , полученных в равновесных условиях методами тензиметрии с мембранным нуль-манометром,  РФА и химического анализа. Определена химическая схема процесса термического разложения борогидридов лантанидов.

Ln (BH4)3== LnB6+LnH2+5.5Н2

С помощью уравнений барограмм рассчитаны термодинамические характеристики процесса и индивидуальных борогидридов некоторых лантанидов, которые приведены в таблице.

Термодинамические характеристики борогидридов лантанидов

| Соеди-нения |  | Термодинамические характеристики |
| --- | --- | --- |
|  | Процесса | разложения | Индивидуальных борогидридов |
|  |  |  |  |  | 32 |  |
|  |  |  |  |  | 30 |  |
|  |  |  |  |  | 40 |  |
|  |  |  |  |  | 32 |  |
|  |  |  |  |  | 42 |  |
|  |  |  |  |  | 29 |  |
|  |  |  |  |  | 29 |  |

THE THERMODINAMIC PROPERTIES OF BORANES LANTANISE.

B.A.Gafurov(1), U.M.Mirsaidov(2), M.S.Islomova(3), A.B.Badalov(3).

1.Kurgantubens government University, Tajikistan, Kurgantube.

2. Agency on nuclear and radiation security of Academy of Science Republic of Tajikistan.

3.    The Tajik Technical University, Tajikistan, Dushanbe.

E-mail: badalovab@mail.ru

Exchange reaction syntheses the salt boranes lanthanide of  in 3THF- 3-tetra hydro furans medium between reaction chloride of lanthanide and    study thermic decomposition of non-salvatere , obtained at  equilibrium conditions by method of the strain measurements with membrane zero-manometer, RFA and chemical analysis.

Determined chemical scheme of thermic decomposition process of borane lanthanide:

Ln (BH4)3== LnB6+LnH2+5.5Н2

The thermodynamic characteristics process and individual borane some of  lanthanide calculated used aguation of barogram’s presented in table.

Thermodynamics characteristics borane  of  lanthanide.

| Substances |  | Thermodynamics characteristics |
| --- | --- | --- |
|  | decomposition | process | Individuals boranes |
|  |  |  |  |  | 32 |  |
|  |  |  |  |  | 30 |  |
|  |  |  |  |  | 40 |  |
|  |  |  |  |  | 32 |  |
|  |  |  |  |  | 42 |  |
|  |  |  |  |  | 29 |  |
|  |  |  |  |  | 29 |  |