THERMAL DECOMPOSITION AND THERMODYNAMIC CHARACTERISTICS OF SULPHATE-URANYL COMPOUNDS

D.D.Kamalov, I.U.Mirsaidov, F.A.Khamidov, A.B.Badalov

Nuclear and Radiation Safety Agency (State Regulatory Authority) of the Academy of Sciences of the Republic of Tajikistan, 33 Rudaki Avenue, 734025, Dushanbe, Tajikistan. Tel: +992 372 27 77 91; Fax: +992 372 21 55 48;

E-mail: badalovab@mail.ru

Thermal decomposition of trihydrate sulphate uranyl is studied by tensimetric methods with the help of zero diaphragm pressure gages, roentgen phase analysis (RFA) and Infra Red Spectroscopy (IRS). The barogram consists of three stages in 300……750 K intervals. Two stages correspond to dehydration process of initial sample and the third corresponds to thermal decomposition of uranyl sulphate.

Equations are compiled and thermodynamic characteristics of separate stages of studied processes are calculated on the basis of these equations.  (Table 1).

Table 1

Equation barogram coefficients and thermodynamic characteristics of dehydration process and UO2SO4∙3H2O decomposition stages.

| Process scheme | ∆T, K | LqPATM = B – A/T ∙ 103 | Thermodynamic characteristics of process |
| --- | --- | --- | --- |
|  |  | A±0.02 | B±0,05 | ∆HoT, kilojoule Mole | ∆SoT, kilojoule Mole | ∆ GoT, kilojoule Mole |
| 1 | 325-370 | 2,92 | 7,39 | 13,34±0,3 | 33,81±0,5 | 2,3±0,3 |
| 2 | 380-420 | 4,45 | 10,84 | 20,36±0,3 | 49,59±0,5 | 1,5±0,3 |
| 3 | 480-750 | 1,42 | 1,86 | 6,49±0,3 | 8,5±0,5 | 2,4±0,3 |

Thermodynamic characteristics of individual sulphate uranyl compounds are calculated on the basis of these equations (table 2)

Table 2

Thermodynamic characteristics of sulphate uranyl compounds

| Compounds | Thermodynamic characteristics of process |
| --- | --- |
|  | – ∆fHoT, kilojoule∙mole -1 | SoT, kilojoule∙mole -1∙K-1 |
|  | Literarure | Experiment | Experiment |
| UO2SO4∙3H2O | 2791,8 | 2383,1±25 | 637,3±42 |
| UO2SO4∙2H2O | - | 2128,0±25 | 482±42 |
| UO2SO4 | 1889,1 | 1624,0±25 | 347±42 |