THERMODYNAMICS OF ORDERING IN LOWER TUNGSTEN CARBIDE W2C

A. S. Kurlov, A. I. Gusev

Institute of Solid State Chemistry, Ural Division of the RAS,

Russia, 620041 Ekaterinburg GSP-145, Pervomaiskaya 91, kurlov@ihim.uran.ru

According to [1], the only ordered phase of the lower hexagonal (space group P63/mmc) tungsten carbide -W2C is the trigonal (space groupP31m) phase -W2C. Besides two superstructures of the carbide -W2C are mentioned in the literature: orthorhombic (space group Pbcn) phase  '-W2C and rhombohedral (space group P3m1) phase  ''-W2C. In this connection, the thermodynamical analysis of phase equilibria in the existence range of the carbide -W2C and its possible superstructures W2tC2t-1 (t = 1) is performed in this study. Phase equilibria are calculated by the order-parameter functional method [2]. The basis cluster s in the form of octahedron comprising six sites of the nonmetallic sublattice with W atom at the center was used for the description of ordering in hexagonal lattice. The free energy of disordered ( = 0) and possible ordered phases with long-range order parameter  was written as

F(y,,T) = F0(T) + yF1(T) + P0(2)F2(T) – TSc(y,) ,

where F0(T), F1(T), F2(T) are the coefficients of the expansion of the free energy of a disordered compound M2Xy (disregarding the configurational entropy Sc) in a power series in y; P0(2)ºP0(2((s)=y2−a(s)h24t2 is the probability of a complete bond C-C for the superstructure discussed; a(s) is a coefficient which depends on the symmetry and type of superstructure; Sc(y,) is the configurational entropy.

Calculations show that trigonal phase -W2C has the lowest free energy at a temperature from 1300 to 2300 K in the homogeneity interval of lower tungsten carbide W2C. Free energy of two other superstructures is higher than the free energy of ordered trigonal phase -W2C therefore  '-W2C and  ''-W2C superstructures cannot exist.

This work is supported by the RFBR (grants 07-03-96066 and 09-03-00010) and by the President’s of the Russian Federation grant MK 805.2008.3.

LITERATURE

[1]  A.S. Kurlov, A.I. Gusev. Phys. Rev. B 76 (2007) 174115.

[2] A.I. Gusev. Nonstoichiometry, Disorder, Short-Range and Long-Range Order in Solids. Nauka - Fizmatlit, Moscow, 2007. 856 pp. (in Russian)