HELIUM PLASMA IMMERSION ION IMPLANTATION OF PET POLYMER

Tóth A.1, Veres M.2, Mohai M.1, Bertóti I.1, Szépvölgyi J.1

1Institute of Materials and Environmental Chemistry, Research Centre for Natural Sciences, Hungarian Academy of Sciences, H-1525 Budapest, P.O. Box 17, Hungary

2Institute for Solid State Physics and Optics, Wigner Research Centre for Physics,
Hungarian Academy of Sciences, H-1525 Budapest, P.O. Box 49, Hungary

E-mail: toth.andras@ttk.mta.hu

Plasma immersion ion implantation (PIII) is a versatile and relatively simple surface modification technique of polymers [1]. The treatment of poly(ethylene terephthalate) (PET) by PIII is of interest, due to the promising applications in packaging (e.g., improvement of gas-barrier properties of beverage-containing PET bottles), and as biomaterial devices (e.g., decrease of bacterial adhesion in cardiovascular implants like heart valve sewing rings and artificial blood vessels) [2-4].

Recently we studied the formation of amorphous carbon type layers on the surface of PET by helium PIII [5,6]. The effect of the main process parameters (acceleration voltage, fluence and fluence rate) on the alterations of the surface chemical composition and structure were investigated by X-ray photoelectron spectroscopy (XPS) and Raman spectroscopy. The relationships obtained offered the possibility of tailoring the chemical structure of the created amorphous carbon layer. Ion-induced changes in properties like colour, wettability and surface electrical resistance were also studied and structure-property and composition-property relationships were obtained. In addition, the He PIII-treated PET system was characterised by two-wavelength Raman spectroscopy, considering also the partially modified structural units [7]. In the top layer, in which the stopping power of PET for He+ ions is dominated by the electronic component, the increase of the portion of aromatic sp2 carbon rings was characteristic. In deeper layers the formation of a crosslinked and disordered structure was deduced, due to the increased nuclear damage at the end of the ion track.

# LITERATURE

[1]	A. Tóth, K. Kereszturi, M. Mohai, I. Bertóti. Surf. Coat. Technol. 204 (2010) 2898.

[2]	M. Ikeyama, S. Miyagawa, S. Nakao, J. Choi, T. Miyajima. Nucl. Instrum. Methods B257 (2007) 741.

[3]	J. Wang, N. Huang, P. Yang, Y.X. Leng, H. Sun, Z.Y. Liu, P.K. Chu. Biomaterials 25 (2004) 3163.

[4]	N. Huang, P. Yang, Y.X. Leng, J. Wang, H. Sun, J.Y. Chen, G.J. Wan. Surf. Coat. Technol. 186 (2004) 218.

[5]	A. Tóth, M. Veres, K. Kereszturi, M. Mohai, I. Bertóti, J. Szépvölgyi. Nucl. Instrum. Meth. B269 (2011) 1855.

[6]	A. Tóth, M. Veres, K. Kereszturi, M. Mohai, I. Bertóti, J. Szépvölgyi. Appl. Surf. Sci. 257 (2011) 10815.

[7]	M. Veres, A. Tóth, M. Mohai, I. Bertóti, J. Szépvölgyi, S. Tóth, L. Himics, M. Koós. Appl. Surf. Sci. (accepted for publication).