PEROVSKITE PHASE FORMATION IN La1-xBaxMn1-yTyO3 (T= Fe, Cr) SYSTEMS

A.N. Petrov

E.A. Filonova, M.Yu. Mitrofanova,

Ural State University, Russian Federation, 620083, Ekaterinburg, Lenina av, 51. helen.filonova@usu.ru

Objects of the present research are doped lanthanum-barium manganites La1-xBaxMn1-yTyO3 (T = Fe, Cr) whose wide studying is caused by potential use as cathode materials for solid oxide fuel cells. The purpose of this work was to study the opportunity for homogeneous phase La1-xBaxMn1-yTyO3 (T = Fe, Cr) obtaining.

The La1-xBaxMn1-yTyO3 (T = Fe, Cr) samples were synthesized on standard ceramic technology in a temperature range 1123-1373К. The phase composition of the products was determined by X-Ray diffraction. Crystal structure determinations of single-phase samples were performed by the Rietveld full-profile method.

Analysis of the phase composition LaMn1-yCryO3, La1-xBaxMnO3 and La1-xBaxMn1-yCryO3 samples have allowed on the phase diagram of LaMnO3-BaMnO3-BaCrO4-LaCrO3 system (fig. 1) to allocate the area of La1-xBaxMn1-yCryO3 solutions with orthorhombical deformed perovskite structure existence (field O) and to allocate the existence area of La1-xBaxMn1-yCryO3 solutions with rhombohedral deformed perovskite structure (field R). Analysis of the phase composition LaMn1-yFeyO3, La1-xBaxFeO3 and La1-xBaxMn1-yFeyO3 samples have allowed on the phase diagram of LaMnO3-BaMnO3-BaFeO2.5-LaFeO3 system (fig. 2) to allocate the area of La1-xBaxMn1-yFeyO3 solutions with orthorhombical deformed perovskite structure existence (field O) and to allocate the existence area of La1-xBaxMn1-yFeyO3 solutions with rhombohedral deformed perovskite structure (field R).

Fig. 1.					Fig. 2.

This work was financially supported by the RFBR (project № 07-03-00076а).