CALORIMETRIC STUDY OF NANOTUBULAR HYDROSILICATES

(Mg,Fe)3Si2O5(OH)4

I.A. Kiselevaa, L.P. Ogorodovaa, E.N. Korytkovab, T.P. Maslennikovab,

V.V. Gusarovb

a Department of Mineralogy, Geological Faculty, M.V.Lomonosov Moscow State University, Russia, 119991, Moscow, Leninskie Gory, MSU

E-mail: kiseleva@geol.msu.ru

b Institute of Silicate Chemistry of Russian Academy of Sciences, Russia, 119155, Saint-Petersburg, Makarov quay, 2

It is of interest to study the mechanisms of nanotubes formation and the determination of the physicochemical conditions of their synthesis. The calorimetric study of synthesized under hydrothermal conditions nanotubular chrysotiles of (Mg,Fe2+,Fe3+)3Si2O5(OH)4 composition was performed on the high-temperature Calvet microcalorimeter “Setaram” (France). The enthalpies of formation of nanotubes studied (table) were determined by “transposed temperature drop solution calorimetry” method at T=973 K in molten 2PbO·B2O3 as a solvent. The heat measured contained two contributions: the heat content of the sample and the enthalpy of solution  [H0(973 K)-H0(298.15 K)+ΔsolH0(973 K)].

Table. The enthalpies of formation of nanotubes studied

| Composition of nanotubes | -ΔfHoel(298.15 K), kJ/mol |
| --- | --- |
| Mg2.88Fe2+0.11Fe3+0.02Si1.99O5(OH)4.0.03H2O | 4283.6±10.1 |
| Mg2.79Fe2+0.22Fe3+0.07Si1.94O5(OH)4.0.10H2O | 4207.9±10.8 |
| Mg2.59Fe2+0.30Fe3+0.11Si1.97O5(OH)4.0.18H2O | 4180.9±13.4 |
| Mg2.30Fe2+0.41Fe3+0.22Si1.98O5(OH)4.0.13H2O | 4144.4±7.3 |
| Mg2.78Fe3+0.20Si1.96O5(OH)4.0.02H2O | 4254.0±7.2 |
| Mg2.66Fe3+0.29Si1.95O5(OH)4.0.01H2O | 4146.7±9.0 |
| Mg2.96Si2.02O5(OH)4.O.66H2O | 4473.7±9.3 |

The enthalpy of formation of magnesium nanotubes is more negative, than this value for Fe-bearing nanotubes. This can likely explains limited character of substitution for magnesium atoms by iron atoms in nanotubes with chrysotile structure in synthesis conditions and in nature.

This study was financially supported by the Russian Foundation for Basic Researches (grants № 08-03-00456, 09-05-00302).