THE ADSORBTION OF ACIDIC GASES WHICH ARE FORMED IN A PROCESS OF PLASMOTHERMIC DETOXICATION OF PHOSPHORORGANIC COMPOUNDS

A.E. Antoshin1, Y.N. Rejhov1, K.V. Tugushov1, N.E. Vaulin2, A.V. Simnanskij2, S.A. Lermontov3, A.N. Malkova3, L.L. Yurkova3

1 Academy of Civilian Defense, Emergence Committee Russia, 144006, Himki Moscow region, Novogorsk. veis444@mail.ru

2 Company “Platex”, Russia, 123027, Moscow, Varshavskoe shosse, 42.

3 Institute of Physiologically Active Compounds of Russian Academy of Sciences, 142432, Moscow region, Chernogolovka, Severnij pr., 1.

We have investigated the reaction of CaO at 620 (C and Ca(OH)2 at 450 (C with a 10:1 mixture of CO2 and SO2.

The total amount of CaCO3+CaSO3+CaSO4 was 66% at 450 (C and 61% at 620 (C. This leads to a conclusion that both CaO and Ca(OH)2 effectively adsorb acidic gases.

We have found that the ratio (CaCO3):(CaSO3 + CaSO4) ≈ 5:1 for the 10:1 mixture at both temperatures. This means that SO2 is absorbed more effectively than CO2 and the excess of carbon dioxide does not prevent sulfur-containing gases adsorbtion.