ADSORPTION OF POLAR MOLECULES ON THE GRAPHITE SURFACE MODIFIED BY MONOMOLECULAR LAYER OF POLAR ANISOMETRIC PARTICLES

S.Yu. Kudryashov

Samara state university, Russia,

443011, Samara, Ak. Pavlova, 1 street, E-mail: kstasu@mail.ru

In this report potential energy of interaction of quasi-solid polar molecule of adsorbate with semi-endless graphite crystal is considered at presence on its surface of a monomolecular layer of polar anisometric particles of the modifier. We have obtained the equation for electrostatic "adsorbate – modifier" interactions energy in the dipole-dipole approaching by transformation the lattice sums:

ΦμμM=2NAabε010-27kν=1∞Μν,0(xk, yk, zk)+μ=1∞Μ0,μ(xk, yk, zk)+2ν=1∞μ=1∞Μν,μ(xk, yk, zk),

where the index k designates modifier molecules in an elementary cell (n, m), aand b – parameters of rectangular elementary cell of modifier monolayer, μ and μMk – dipole moments of adsorbate and modifier molecules, rkmn – distance between interacting molecules, xk=xo−xko, yk=yo−yko, zk=zo−zko, xko, yko, zko – mass center coordinates of the k-th modifier molecule, xo, yo and zo – mass center coordinates of the analyte in the coordinates system connected with adsorbent, the dipoles centers coincide with the molecules mass centers, auxiliary functions Μν,μ(x, y, z)have the form:

Μν,μ(x, y, z)=uν,μexp(−2uν, μz)[(μxμMkxuν,02uν,μ2+μyμMkyu0, μ2uν, μ2−μzμMz)cos(2uν,0x)cos(2u0,μy)−−(μxμMky+μyμMkx)uν,0u0,μuν,μ2sin(2uν, 0x)sin(2u0,μy)−(μxμMkz+μzμMkx)uν, 0uν, μsin(2uν, 0x)cos(2u0,μy)−−(μyμMkz+μzμMky)u0,μuν,μcos(2uν,0x)sin(2u0,μy)],

where uν,μ2=π2ν2/a2+π2μ2/b2.

Lennard-Jones (6, 12) potentials are used for the description of dispersive interactions. It is shown, that the formula, suitable for practical calculation of potential energy of "adsorbate – adsorbent" interactions, may be received if we will model monolayer of the modifier impenetrable for adsorbate with the power centers forming a plane lattice with translation periodicity, and the power centers uniform distributed in plane, parallel outward verge of a graphite crystal.