ДИАГРАММА СОСТОЯНИЯ СИСТЕМЫ Fe-Ge-O

ПРИ 1050 – 1300 К

# С.В. Штин, А.А. Лыкасов, А.А. Кимяшов

Южно-Уральский государственный университет,

пр. Ленина76, 454080, г. Челябинск, Россия

swet@fizchim.susu.ac.ru

Для построения фазовой диаграммы системы железо-германий-кислород использовали метод измерения ЭДС концентрационного по кислороду гальванического элемента с твердым электролитом. Один из электродов в таком элементе – исследуемое вещество, второй электрод – равновесная смесь железа и вюстита (электрод сравнения).

Образцы были приготовлены из порошков железа, Fe2O3 и GeO2 методом твердофазной реакции. Для подтверждения фазового и химического состава был проведен электрозондовый микроанализ.

ЭДС элементов измеряли в интервале температур 1050 – 1300 К. На основании полученных экспериментальных данных были рассчитаны значения и построены зависимости равновесного парциального давления кислорода от состава образцов (с или у) в исследуемом интервале температур. Эти зависимости позволили построить коноды в двухфазных областях и изобары кислорода в области существования гомогенного германийзамещенного вюстита. По пересечению конод и изобар определены координаты границ фазовых областей. Изотермическое сечение диаграммы при 1273 К приведено на рис.1. В системе наблюдается высокая растворимость германия в железе. Раствор германия в -железе обозначен на диаграмме . Фаза  – раствор на основе химического соединения Fe3Ge, фаза  – на основе химического соединения Fe3,2Ge2. Раствор германия в вюстите обозначен на диаграмме W. Растворимость германия в вюстите при 1273 К составляет не более 0,3 мол.%.

В системе имеются две шпинели стехиометрического состава –  и , которые образуют два шпинельных раствора, обозначенных на диаграмме  и . Расслоение шпинельного раствора – на  и  подтверждается термодинамическими данными и результатами электронно-зондового микроанализа.

PHASE DIAGRAM OF Fe-Ge-O SYSTEM

AT 1050 – 1300 K

# S.V. SHTIN, А.А. LYKASSOV, А.А. КIMYASHOV

South Ural StateUuniversity,

Lenin av. 76, 454080, Chelyabinsk, Russia

swet@fizchim.susu.ac.ru

The phase diagram of Fe-Ge-O system was constructed, using the galvanic cell EMF measurement method the with solid oxygen-containing electrolyte. One electrode was research sample. equilibrium iron – wustite mixture was used as standard electrode.

Samples have been prepared from Fe, Fe2O3 and GeO2 powders by a method of solidphase reaction. For defining of phase and chemical compound has been lead electrosonde microanalysis.

The EMF of the galvanic cell was measured at 1050 – 1300 K. The dependence partial oxygen pressure vs composition has been determined in this temperature range according with results of measuring of the EMF. Conoids in two-phases regions and isobar of oxygen in Ge-substitution wustite region has been construct, using this dependences. The phase regions boundaries have been determined by conoids and isobars crossing. Phase diagram of Fe-Ge-O system is shone at fig.1. Ge is very good dissolved in the iron. -phase is the solid of Ge and -Fe. The -phase is Ge-solution in Fe3Ge. The -phase is Ge-solution in Fe3,2Ge2. Ge-solution in wustite designated on the diagram as W. Ge-solubility in wustite is 0,3 mole% at 1273 K.

In this system there are two spinel phases –  and . They have been formed two spinel solution, designated on the diagram are  and . The dissolving spinel solution – on  and  have been confirmed by thermodynamic data and electrosonde microanalysis results.