PHASE STABILITY, OXYGEN NONSTOICHIOMETRY AND THERMAL PROPERTIES OF THE LnBaCo2O5+ (Ln = Nd, Sm, Eu, Tb, Y) LAYERED PEROVSKITES

T.V. Aksenova, A.S. Podzorova, L.Ya. Gavrilova, V.A. Cherepanov

Ural State University, Russia, 620083, Yekaterinburg, Lenin av., 51,

E-mail: aksenovatanya@yandex.ru

The crystal structure and physicochemical properties of the LnBaCo2O5+ (Ln = Nd, Sm, Eu, Tb, Y) layered perovskite-type complex oxides were studied in the present work.

The syntheses of the samples under investigation were carried out using conventional ceramic route and glycine-nitrate method. Final anneal was performed at 1373 K in air with following slow cooling to room temperature. Phase identification and crystal structure studies were made by means of X-ray and neutron diffraction methods. Oxygen nonstoichiometry () of the complex oxides LnBaCo2O5+ was studied by TGA method within the temperature range 273T, K1373 in air.

It was shown that the crystal structure of LnBaCo2O5+ layered perovskites considerably depends on radii of rare earth element and oxygen content. X-ray diffraction pattern of NdBaCo2O5+ was indexing within tetragonal unit cell apap2ap, P4/mmm space group (=0.62), where ap – is the unit cell parameter of the cubic perovskite. Doubling of the parameter c caused by the alternation of the layers containing neodymium and barium ions. The decrease of rare earth atom size leads to the decrease of  (0.42≤<0.62), and X-ray diffraction patterns for LnBaCo2O5+ (Ln = Sm, Eu, Tb) reveals splitting of the peaks at 22.72 and 46.47 that indicate change of symmetry and transformation to orthorhombic unit cell ap2ap2ap, Pmmm space group. The doubling of parameter b caused by the ordering of oxygen vacancies located in the layers containing rare earth ions. Meanwhile, the crystal structure of YBaCo2O5+ with the smallest from all rare earth yttrium ion better described in tetragonal symmetry with triple a and b parameters 3ap3ap2ap within P4/mmm space group (<0.4).

Thermal expansion coefficients for all cobaltites were measured with the help of Netzsch DIL 402C dilatometer at the temperature range 298 – 1273 K in air. Monotonous shape of L/L=(T) curves prove an absence of phase transitions within studied temperature range in air.

This work was financially supported in parts by Russian Federation President grant № MK-3162.2008.3; RFBR grants № 07-03-96079 and № 09-03-00620.