Dissociation Energies of MnO, FeO, CoO, NiO Molecules1).

E.K. Kazenas, Yu. V. Tsvetkov, N.V. Polikarpova

Baikov Institute of Metallurgy and Material Science, RAS

(Leninskii pr. 49, 119991, Moscow, Russia)

# E-mail: kazenas@ultra.imet.ac.ru

The  gas phase above MnO, FeO, CoO, NiO oxide at 1800 K consists of Me(г); O2(г), O(г), and MeO(г). The content of faseous oxides in the gas phase at 1800 K is (%):MnO(г) (7,3);  FeO(г) (2,5); CoO(г) (1,1); NiO(г) (1,2). Basing on the measurements of partial pressure of Mn, Fe, Co, Ni oxides the enthalpies of sublimation, formation and the dissociation energies of gaseous molecules of the oxides were determined. (See Table)

Table.

Sublimation and formation enthalpies, dissociation energies of gaseous oxide molecules ((D H, D  kJ/mol   +  4 kJ/mol)

| Compound, measuring interval(Т.К) | D Hos,298 MeO(г) | Do298 MeO(г) | D Ho f,298 MeO(г) |
| --- | --- | --- | --- |
| MnO 1630-1815 | 503,3 | 410,9 | 122,5 |
| FeO 1930-1950 | 542,9 | 407,5 | 257,9 |
| CoO 1615-1820 | 556,3 | 1362,4 | 320,2 |
| NiO 1143-1293 | 550,9 | 367,4 | 311,4 |

1) The work was financially supported by the project of President of RF.

(grant НШ 2991.2008.3).