PHASE RELATIONSHIPS, MIXED CONDUCTIVITY, MÖSSBAUER SPECTRA AND THERMAL EXPANSION IN THE (La,Sr)(Fe,Ni)O3–δ SYSTEM

E.A. Kiselev1, E.V. Tsipis2,3, V.A. Kolotygin3, J.C. Waerenborgh2,
V.A. Cherepanov1, V.V. Kharton3

1Ural State University, Russia, 620083 Yekaterinburg, Lenin av. 51

2Instituto Tecnológico e Nuclear, Portugal, 2686-953 Sacavém, CFMC-UL, EN 10

3CICECO, University of Aveiro, Portugal, 3810-193 Aveiro, kharton@ua.pt

The incorporation of Sr2+ in perovskite-type La1−ySryFe1−xNixO3−δ increases oxygen deficiency and ionic transport at elevated temperatures, but leads to a lower thermodynamic stability as reflected by narrowing the solid-solution domain at 1373 K down to x≈0.25 at y=0.10 and x≈0.12 at y=0.20 in air. The average thermal expansion coefficients of La1−ySryFe1−xNixO3−δ (x=0.1–0.4, y=0.1–0.2) ceramics vary in the ranges (12.4–13.4)×10−6 K−1 at 700–1150 K and (14.2–18.0)×10−6 K−1 at 1150–1370 K, rising with strontium and nickel contents. These additives lower also the temperature of orthorhombic→rhombohedral phase transition visible in the dilatometric curves, promote hole delocalization, increase total conductivity and decrease Seebeck coefficient studied in the oxygen partial pressure range from 10−5 to 0.4 atm at 973–1223 K. The steady-state oxygen permeation fluxes through single-phase La1−ySryFe1−xNixO3−δ (x=0.1–0.2, y=0.1–0.2) membranes, with an activation energy of 206–235 kJ/mol, are determined by both surface-exchange and bulk ionic conduction limited by the oxygen-vacancy concentration. Doping with nickel has a weak negative effect on the oxygen transport, probably due to defect cluster formation involving the vacancies and Ni2+. On the contrary, at low temperatures when (La,Sr)(Fe,Ni)O3−δ becomes almost oxygen-stoichiometric in air, the Mössbauer spectroscopy and thermogravimetric analysis showed that the average oxidation state of nickel is higher than +3, similar to iron cations.

This work was supported by the FCT, Portugal (projects PTDC/CTM/64357/2006 and SFRH/BPD/28629/2006), and the Russian Federal Agency on Science and Innovations (state contract No. 02.444.11.7020).