VAPORIZATION THERMODYNAMICS OF EUROPIUM DIBROMIDE

M.F. Butmana, D.N. Sergeeva, V.B. Motalova, L.S. Kudina, L. Rycerzb,

M. Gaune-Escardc

a Ivanovo State University of Chemistry and Technology, Engelsa 7, 153000 Ivanovo, Russia butman@isuct.ru

b Chemical Metallurgy Group, Faculty of Chemistry, Wroclaw University of Technology, Wybrzeze Wyspianskiego 27, 50-370 Wroclaw, Poland

c Ecole Polytechnique, Mecanique Energetique, Technopole de Chateau-Gombert, 5 rue Enrico Fermi, 13453 Marseille Cedex 13, France

The vaporization of europium dibromide (99.9%) was studied by high temperature mass spectrometry. Temperature dependences of ion currents are presented in Fig. 1. The partial pressure of molecules EuBr2 in the saturated vapor was determined to be (1049-1261 K): ln p(EuBr2)Pa = (-36.224 ± 0.643) ×103/T + (18.611 ± 0.558). It was found that the fraction of dimers Eu2Br4 does not exceed 1 %. In Fig. 2 experimental data on temperature dependence of heat capacity, Cop, of EuBr2 obtained by the differential scanning calorimetry in the temperature range of 300-1100 K are shown. For crystal EuBr2 Cop = 73.79 + 8 T (± 2.25) J mol-1 K-1. For liquid EuBr2 Cop = 105.39 ± 3.32 J mol-1 K-1. The temperature and enthalpy of fusion are 941 K and 22.2 ± 0.4 kJ mol-1 respectively. The thermodynamic characteristics of evaporation/sublimation of EuBr2 were determined with the use of calculated thermodynamic functions of EuBr2 in the gaseous («rigid rotator–harmonic oscillator» approach, molecular parameters were taken from [1]) and condensed phases by the IInd and IIIrd laws techniques. The comparative analysis of available literature data on the saturated vapor pressure of EuBr2 was carried out. The enthalpy of reaction EuBr2, cr. = EuBr2 was recommended to be sH(298.15 K) = 354  5 kJ mol-1.

| Fig. 1. Temperature dependences of ion currents | Fig. 2 Temperature dependence of molar heat capacity of EuBr2 |
| --- | --- |

REFERENCES

[1] N.I. Giricheva, G.V. Girichev, S.A. Shlykov, O.V. Pelipets. Zhurn. struct. khim. 45 (2004) 50.

This work was granted by RFBR, project No. 09-03-97536.