INITIAL RATE OF SOLID STATE REACTIONS AND COMPOSITION OF THE REACTIONARY MIXTURE

V.G.Povarov, O.B.Sokolova

The Russian state pedagogical university, faculty of chemistry, Russia, Petersburg, emb. of Moika, B. 48, povarovvg@rambler.ru

Rate of solid state reactions is influenced with a lot of factors: by dispersion degree of reagents, temperature, pressure, mode of preparation of reagents, a way of preparation of a reactionary mixture and its composition [1, 2]. Where are some difficulties at studying last problem. At first, only for stechiometric mixtures of reagents their ratio does not change during reaction [2]. At second, accumulation of solid products of reaction also change kinetic laws. It is correct to take into account influence of structure of a reactionary mixture on solid state kinetic by investigation of initial rate from initial composition of system. Results of experimental measurements of initial rate in six systems 1)Na2CO3+V2O52NaVO3+CO2, 2)Na2CO3+Fe2O3Na2Fe2O4+CO2, 3)Na2CO3+2AgCl2NaCl+2Ag+CO2+0.5O2, 4)Zn+PbCl2Pb+ZnCl2, 5) Zn+NiCl2Ni+ZnCl2, 6)2AgCl+Zn2Ag+ZnCl2 are presented at various temperatures. Rate was measured in first three systems by the loss of weight of a sample  for 2-5 minutes. In systems 4 and 6 rate measured by chloride of zinc by a mode of complex titrations. For system with nickel used magnetic mode (on nickel). The initial weight of sample was 0.1 - 0.2 g. In all systems rate were measured in 5 mixtures at initial molar ratio of reagents 3:1, 2:1, 1:1, 1:2, 1:3. In all cases the minimum of a degree of transformation is found out at stechiometric ratio of reagents. The similar data have been received in work [3] for reactions CaCO3+MoO3CaMoO4+CO2 and 2Li2CO3+LiFe5O85LiFeO2+2CO2. For dependence of a degree of transformation from initial composition was received expression:			Z(XA)=tXA(1−XА)αΔM∞U=p'XA(1mA−1mB)+1mB

t- is time of experiment, XA- is molar fraction of reagent A, M- is the quantity of  product formed at the end of reaction, p’- is a factor of proportionality, mA- is a quantity of reagent A in one grain of a reagent, mB - is amount of reagent B in one grain of a reagent, U- is a molar volume of a reactionary mixture.

LITERATURE:

[1]. Tretikov  Yu.D. Solid state reactions. M.: 1978, 134 p.

[2]. Povarov V.G., Blandur E.P. // Kinetics and catalysis 1999, 40, № 4, P. 520-524.

[3].Povarov V.G. //Bulletin of Petersburg State University. 2001,  №20, P. 54- 61.