CALCULATION OF HYDROGEN SOLUBILITY 
IN IRON-VANADIUM ALLOYS

K.Yu. Okishev, D.A. Mirzayev

Southern Ural State University, Russia,
454080, Chelyabinsk, pr. Lenina, 76. E-mail: mirzayev@physmet.susu.ac.ru

The following equation of hydrogen solubility in iron-vanadium alloys is obtained based on M.A.Shtremel’s theory of short-range ordering [1] concerning pair interactions of nearest neighbours in substitutional and interstitial sublattices:

, cm3/100 g,

where z=4 is the number of metal atoms surrounding a hydrogen atom located in a tetrahedral interstice of b.c.c. lattice; V is atomic fraction of vanadium in metal sublattice;  is hydrogen pressure in atmospheres, and  is the difference of interaction energies of hydrogen atoms with vanadium and iron atoms. Calculated values correspond well with experimental data cited in [2] at , J/mol (fig. 1). Hydrogen solubility was well described in [2] in the long-range order model, but vanadium does not form a superlattice structure with iron, and in our opinion the short-range order model should be more close to reality.

Fig. 1. Dependence of hydrogen solubility in Fe-V alloys on vanadium concentration 
at 773 (1), 873 (2), 973 (3) и 1073 К (4)

REFERENCES

[1] M.A. Shtremel, Yu.A. Krupin, Ye.B. Zaretski. Phys. Met. Metallogr. 46 (1978) 984.

[2] Z.A. Matysina, M.I. Milyan. Metally (1990, No. 2) 175.