physicochemical characteristics of betulin prepared by supercritical fluid extraction

V.F. Uryash1, N.Yu. Kokurina1, А.E. Gruzdeva2, L.А. Faminskaya1,

А.V. Uryash3, I.N. Kalashnikov1

1Research Institute of Chemistry Nizhny Novgorod State University, Gagarin Pr., 23/5, Nizhny Novgorod, Russia

E-mail: ltch@ichem.unn.ru

2ООО “Grande”, Krasnie Zori Str., 24/5, Nizhny Novgorod, Russia

E-mail: bio_nn@mail.ru

3Mount Sinai Medical Center, Department of Research, Miami Beach, Florida, USA

E-mail: auryash@msmc.com

Betulin is a natural biologically active substance that is a pentacyclic triterpene alcohol of lupane row. Its gross formula is С30Н50О2; М=442.7 g/mol. Betulin posseses antiseptic, antiviral, bile-expelling, gastro- and hepatoprotective action. It was isolated from СО2-extract of birch bark. The content of the main substance in it amounted to 97%. The extraction of birch bark with supercritical СО2 was performed at Т=313 K and pressure Р=15.0 mPa according to the patented technology [1] on an UEN unit designed with the scientific-production company ZAO “Biofit” (Nizhny Novgorod).

The heat capacity of betulin was measured by us in a vacuum adiabatic calorimeter in the range 80-330 K and its differential thermal analysis was conducted between 80 and 550 K. A transition of endothermal character – a relatively sharp deviation of a base line from a zero trend connected with an increase in the heat capacity of a sample - appeared on the thermogram of betulin in the interval 220-260 K. In accordance with Westrum – McCullough classification such transitions in crystalline substances are considered as glassy ones (G-type). A mean temperature of the transition interval is ТG=246 K. Then an exothermal peak of transition to crystals stable in the given temperature range was seen at 433 K and an endothermal peak of their fusion was recorded at 524 K.

The work was carried out with financial support of the RFBR (grant No 08-03-97052 r_povolzhie_a).

# References

1. Gruzdeva А.E., Grishatova N.V., Demidik M.M., Yakubova I.Sh., Levachev O.S., Chesnokova T.А., Zakamennykh Т.N., Тyulina N.Е., Solomakha K.G. Patent of RF, No 2264442, 20.11.2005.