SUPRAMOLECULAR ASSEMBLING OF INCLUSION COMPLEXES COMPOSED OF CYCLODEXTRINS AND MODIFIED

POLY(DIMETHYL SILOXANE)

M.P. Sokolova1, S.V. Bronnikov1, T.E. Sukhanova1, V. Harabagiu2

1Institute of Macromolecular Compounds of the Russian Academy of Sciences, Russia,  Bolshoi Prospekt 31, 199004 St. Petersburg

2“Petru Poni” Institute of Macromolecular Chemistry, Romania, Aleea Grigore Ghica Voda 41A, 700487 Iasi

pmarip@mail.ru

During last years, much attention has been paid for systems based on self-assembling and self-organization. Examples of such systems are supramolecular inclusion complexes (SICs). SICs are composed of macrocycles (the host) threaded through linear molecules (the guest). There are no covalent interactions between their linear and cyclic components [1-3]. SICs have already been used in different practical applications as controlled molecular switchers [4], for the oral drug delivery systems [5] and as templates for generation of porous silica materials [6], etc.

In the present study, - and γ-cyclodextrin (- and γ-CD) as the host molecules and modified poly(dimethyl siloxane) (E-PDMSs) of different molecular weights as guest macromolecules were used for SICs preparation.

The morphology of SICs based either - or γ-CDs and PDMS of different molecular weighs was examined by scanning electron microscopy (SEM).

The structural entities were described with the model of reversible aggregation [7, 8]. Based on principles of the equlibrium irreversible thermodynamics. Using this model, statistical distributions of crystalline entities have been successful described.This evidences formation of the optimized thermodynamic statistical ensembles of the crystalline entities.

The morphology of the SICs was found to depend on conditions of the complex synthesis, components purification and ratio between components.

This work was supported by Russian Foundation for Basic Research Grant 07-03-91681.

ЛИТЕРАТУРА

1.	G. Schill, Catenanes, rotaxanes, and knots, New York & London: Acad. Press, 1971.

2.	I.G. Panova, I.N. Topchieva, Russ. Chem. Rev. 70 (2001) 23.

3.	F. Huang, H.W. Gibson, Progr. Pоlym. Sci. 30 (2005) 982.

4.	V. Balzani, M. Gumez-Lipez, J.F. Stoddart, Acc. Chem. Res. 31 (1998) 405.

5.	T. Ooya, M. Eguchi, A. Ozaki, N. Yui, Int. J. Pharm. 242 (2002) 47.

6.	B.H. Han, M. Antonietti, Chem. Mater. 14 (2002) 3477.

7.	H.G. Kilian, R. Metzler, B. Zink, J. Chem. Phys. 107 (1997) 8697.

8.	H.G. Kilian, S. Bronnikov, T. Sukhanova, J. Phys. Chem. B. 107 (2003) 13575.