Standard thermodynamic properties intermetallic compounds in the system Ag–Sb

M.V. Voronin1, K.A. Ionov2, E.G. Osadchii1

1Institute of Experimental Mineralogy RAS, Russia, 142432, Chernogolovka, Moscow region, Institutskaya ul., 4. E-mail: voronin@iem.ac.ru

2Dubna International University of Nature, Society, and Man, Russia, 141980, Dubna, Moscow region, Universitetskaya ul., 19.

Two intermetallic compounds (minerals) are well-known in the system Ag–Sb [1]: Ag6Sb (allargentum), Ag3Sb (dyscrasite). Multiplicity measurements were carried out using EMF-method for determination of these phases thermodynamic properties [2, references therein]. Thermodynamic constants are not specified for these compounds in modern handbooks of thermodynamic values.

The three electrochemical reactions were carried out in the system:

- reaction of dyscrasite’s formation from elements;

- reaction of allargentum’s formation from dyscrasite;

- also it is possible to measure reaction (1) relatively reaction (2) in symmetrical electrochemical cell.

Free energy, entropy and enthalpy of reactions were calculated using basic equations of thermodynamic from temperature EMF (E) dependences, obtained in the galvanic cells. Our results and literature data are presented in the table 1.

Table 1. Standard thermodynamic properties of compounds in the system Ag–Sb.

| Compound | ΔfG, kJ·mol-1 | S, J·K-1·mol-1 | ΔfH, kJ·mol-1 | Reference |
| --- | --- | --- | --- | --- |
| Ag3Sb | -5.78 | 196.36 | 1.13 | this study |
|  | -7.2 | 151.61 | -0.52 | 3 |
|  | - | 171.54 | 23.01 | 4 |
| Ag6Sb | -6.34 | 333.21 | 3.31 | this study |

The study was executed with financial support of the RFBR (grants №№ 08-05-00564, 08-05-00582) and program № 7 of the Earth Science Department of RAS.

references

[1] H. Okamoto. J. of Phase Equilibria and Diffusion 28 (2007) 403.

[2] E.G. Osadchii et al. Phys Chem Minerals 25 (1998) 288.

[3] G. Lukashenko et al. Zh. Neorg. Khim. (1964) №9 220 [in Russian].

[4] M.K. Karapetyants, M.L. Karapetyants. Basic Thermodynamic Constants of Inorganic and Organic Compounds. Chemistry Press, Moscow, 1968 [in Russian].