ELECTROCHEMICAL METHODS OF DEFINITION THE THERMODYNAMIC CHARACTERISTICS OF FORMATION PHASES ON THE BASIS OF MeLn2S4 (Me - Ca, Ba; Ln - Nd, Gd, Yb, Sm)

L.A. Kalinina, Ju.N. Ushakova, B.A. Ananchenko,

O.V. Medvedeva, T.V. Mikhailichenko

SEI OF HPE «Vyatka State University», Kirov, Russia, kla500@yandex.ru

The results and prospects of use electrochemical methods (EM) of definition the thermodynamic characteristics of formation complex nonstoichiometric phases on the basis of ternary sulfides MeLn2S4, known as sulfide conductive solid electrolytes (SE) are discussed. The nonconventional methods of measurement of EMF in concentration cells with transfer in the electrolytic temperature interval are offered. Research of the temperature dependence EMF at variation of structure of electrolytes and electrodes allow to make thermodynamic testing: 1) reactions of formation ternary MeLn2S4 from binary MeS and Ln2S3; 2) processes of dissolution of binary sulfides in appropriate ternary MeLn2S4.

The thermodynamic properties of the tested reactions are determined and ΔHLn2S3 of ternary sulfides are calculated (table 1).

Table 1 - Formation enthalpy of some sulfide conductive SE

| Currentforma-tion reaction | ΔH6730±5 kJ/mol | Substance (SE) | ST | −ΔHf,2980±125 kJ/mol | T, К | , Smsm-1 |
| --- | --- | --- | --- | --- | --- | --- |
| CaS+Sm2S3 | -260 | CaSm2S4 | Th3P4 | 1930 | 623-773 | 10-5-10-4 |
| CaS+Gd2S3 | 23 | CaGd2S4 | Th3P4 | 1575 | 623-753 | 10-5-10-4 |
| BaS+Sm2S3 | 154 | BaSm2S4 | CaFe2O4 | 1530 | 623-723 | 10-4-10-3 |
| CaS+Yb2S3 | 346 | CaYb2S4 | Yb3S4 | 1307 | 459-779 | 10-4-10-3 |

The activity of binary MeS and Ln2S3 in solid solutions on the basis of MeLn2S4 are determined. The character of activity change of Ln2S3 (Ln – Nd, Gd, Yb) depending on their contents in the appropriate CaLn2S4 differs from character of the appropriate dependence for Ca(Ba)Sm2S4, but as a whole does not contradict the phenomenological theory of ionic transfer in solid electrolytes. The change of the partial mole enthalpy ΔHLn2S3 depending on structure of solid solutions is characteristic for the vacancy mechanism of defect formation in the investigated phases.