THERMODYNAMIC RESEARCH OF THE Tl(Ag)-Sb-S SYSTEMS

BY METHOD EMF

Y.I.Jafarov, N.B.Babanly, Yu.A.Yusibov,  M.B Babanly

Baku, Azerbaijan, AZ1148, Z.Khalilova, 23, Baku State University

Babanly_mb@rambler.ru

The results of complex research of phase equilibria and thermodynamic properties of the systems Tl(Ag)-Sb-S by using DTA and X-ray analyses, also measurement of micro hardness and EMF of concentration chains of type

(-) Tl (s) / liquid electrolyte + Tl + /(Tl-Sb-S) (s) (+)                          (1)

(-) Ag (s) / Ag4RbI5 (s) / (Аg-Sb-S) (s) (+)                                  (2)

at  300-380 K temperature interval are submitted in this activity.

In chains (1) as electrolyte is used the glycerin solution of KCl with addition TlCl, in chains (2) – solid electrolyte Ag5RbI5, having pure ionic conductivity on cation Ag+.

The T-x-y diagrams of the above-stated systems, several vertical sections and isothermal section at 300K were constructed. The area of primary crystallization, types and coordinates of non-variant equilibriums are determined.

From the results of EMF measurements of chains type (1) and (2) the partial thermodynamic functions of thallium and silver are calculated. With the aid of relative partial molar functions in conformity with the phase diagrams of corresponding systems are calculated the standard integrate thermodynamic functions of ternary compounds (table).

Standard integral thermodynamic functions of thallium and silver tiostybnites

| Phase | −ΔG2980 | −ΔH2980 | S2980, J/(molK) |
| --- | --- | --- | --- |
|  | kJ/mol |  |  |
| TlSb5S8 | 481,124,2 | 489,622,7 | 519±20 |
| TlSb3S5 | 314,214,7 | 320,814,5 | 339±15 |
| TlSbS3 | 146,75,0 | 149,75,5 | 196±7 |
| TlSbS2 | 146,35,1 | 152,26,0 | 154±7 |
| Tl3SbS4 | 258,45,7 | 264,410,3 | 346±10 |
| Tl3SbS3 | 253,69,1 | 259,99,9 | 313±12 |
| AgSbS2 | 110,04,8 | 103,15,0 | 1757 |
| Ag3SbS3 | 153,25,1 | 141,26,8 | 30913 |
| Ag7SbS6 | 232,97,2 | 217,812,1 | 59528 |
| Ag5SbS4 | 192,85,9 | 179,59,3 | 43120 |

ТЕРМОДИНАМИЧЕСКОЕ ИССЛЕДОВАНИЕ СИСТЕМ Tl(Ag)-Sb-S МЕТОДОМ ЭДС

Я.И.Джафаров, Н.Б.Бабанлы, Ю.А.Юсибов, М.Б.Бабанлы

Баку, Азербайджан, AZ1148, З.Халилова, 23, БГУ

Babanly_mb@rambler.ru

В даной работе представлены результаты комплексного изучения фазовых равновесий и термодинамических свойств систем Tl(Ag)-Sb-S методами ДТА, РФА, а также измерением микротвердости и ЭДС концентрационных цепей типов

(-) Tl (тв) / жидкий электролит + Tl + / (Tl-Sb-S) (тв) (+)                          (1)

(-) Ag (тв) / Ag4RbI5 (тв) / (Аg-Sb-S) (тв) (+)                                  (2)

в интервале 300-380 K.

В цепях (1) в качестве электролита был использован глицериновый раствор KCl с добавлением TlCl, а в цепях (2)- твердый электролит Ag5RbI5 с чистой ионной проводимостью по катиону Ag+.

Построены полные Т-х-у диаграммы указанных систем, их различные вертикальные сечения и изотермические сечения при 300 К. Определены поля первичной кристаллизации, типы и координаты нонвариантных равновесий.

Из результатов измерений ЭДС цепей типа (1) и (2) были рассчитаны парциальные термодинамические функции таллия и серебра. С помощью относительных парциальных молярных функций в соответствии с фазовыми диаграммами соответствующих систем вычислены стандартные интегральные термодинамические функции тройных соединений (таблица).

Стандартные интегральные термодинамические функции тиостибнитов Tl и Ag

| Фаза | −ΔG2980 | −ΔH2980 | S2980, Дж/(мольК) |
| --- | --- | --- | --- |
|  | кДж/моль |  |  |
| TlSb5S8 | 481,124,2 | 489,622,7 | 519±20 |
| TlSb3S5 | 314,214,7 | 320,814,5 | 339±15 |
| TlSbS3 | 146,75,0 | 149,75,5 | 196±7 |
| TlSbS2 | 146,35,1 | 152,26,0 | 154±7 |
| Tl3SbS4 | 258,45,7 | 264,410,3 | 346±10 |
| Tl3SbS3 | 253,69,1 | 259,99,9 | 313±12 |
| AgSbS2 | 110,04,8 | 103,15,0 | 1757 |
| Ag3SbS3 | 153,25,1 | 141,26,8 | 30913 |
| Ag7SbS6 | 232,97,2 | 217,812,1 | 59528 |
| Ag5SbS4 | 192,85,9 | 179,59,3 | 43120 |