Lyotropic phase behaviour and physical – chemical properties OF lanthanidE CONTAINING nematogens

A.I. Galeevaa, N.M. Selivanovaa, Yu.G. Galyametdinova,b

aKazan State Technological University,

Russian Federation, 420015 Kazan, K.Marks st, 68.

bKazan Physicotechnical Institute, KSC RAS,

Russian Federation, 420029 Kazan, Sibirskii trakt 10/7.

Е-mail: galeeva-alija@mail.ru

Lyotropic liquid crystals have been receiving increased attention in the past decade due to its extensive applications in the field of catalysis, electronics, biotechnology, nanotechnology [1].

In this work we presented lyotropic phase behavior in systems of N,N-dimethyldodecylamine-N-oxide (DMAO)/Lа(NO3)3∙6H2O/water/decanol. The phase diagram was constructed by using polarization optical microscopy (Fig. 1). Concentration and temperature interval of existence and types of liquid crystal phases were established. Hexagonal, lamellar and nematic were detected by microscopic texture observation. It is important note that lyotropic-nematic phases exist from 15оС, till room temperature and above. It is showed that addition of surfactant to the system increase the temperature of mesophase transition to isotropic liquid. The maximum value of phase transition mesophase – the isotropic liquid is characteristic for systems at surfactant:metal 3:1, and makes Т=107оС.

Fig. 1. The phase diagrams of systems DMAO/Lа(NO3)3∙6H2O/water/decanol. The observed types of lyotropic liquid crystal phases are designated: – hexagonal phase, – lamellar phase, – nematic phase.

80

70

60

50

40

70

20

40

60

70

30

50

C10H21O

10

20

30

40

50

H2O

30

30

100,8°С

106,7°С

103,8°С

62,8°С

30°С

44,8°С

105,6°С

107°С

104°С

90,8°С

68,9°С

50,8°С

97,6°С

107°С

79,6°С

10

H2O

2:1

С12DMAO:La(III)

3:1

С12DMAO:La(III)

Structure changes in the system DMAO/Lа(NO3)3∙6H2O/water/decanol (45 wt.%/50 wt.%/5 wt.%, molar ratio surfactant:metal 3:1) in temperature interval 283-358 K. have been determined using viscosimetry. Good correlation of experimental data of different methods for the phase transition analysis has been exhibited.

This work was financially supported by grant RFBR № 08-03-00984-а.

references

[1] M.E. Raimondi, J.M. Seddon Liquid Crystals. 26 (1999) 305.