THERMAL CAPACITY OF MANGANITES LaMeIMeIIMn2O6

(MeI-Li, Na, K, Rb; MeII-Mg, Ca, Ba) in the range 298,15-673 К

Zh.S. Bekturganov

JSC «Research-and-Production Center «Phytochemistry»

4 Gazaliev str., Karagamda, Kazakhstan, 100009

Е-mail: phytoinform@nursat.kz

Discovery of giant negative magnetoresistance in manganites like La1-x(Ca, Ba)xMnO3 in 1993-1994 laid the foundation for intense researches to find and studies of physical and chemical properties in similar. In this regard, we were the first to synthesize a series of triple manganites with the composition LaMeIMeIIMn2O6 (MeI-alkaline; MeII-alkali earth metals). This paper generalizes the results of our calorimetric studies to find С0рf (Т) dependence on IT-C-400 apparatus (Table).

| Manganite | Equation coefficients С0р=a+вT+cT-2, J/molК |  |  | Т, К |
| --- | --- | --- | --- | --- |
|  | а | в 10-3 | с 105 |  |
| LaLiMgMn2O6 | 2049 | 26212 | 11,30,5 | 298,15-673 |
| LaLiSrMn2O6 | 1937 | 27211 | 24,70,9 | 298,15-673 |
| LaLiBaMn2O6 | 33518 | 1498 | 94,25,0 | 298,15-673 |
| LaNaMgMn2O6 | 20910 | 27013 | 8,50,4 | 298,15-673 |
| LaNaCaMn2O6 | 1266 | 32515 | 5,60,3 | 298,15-673 |
| LaNaBaMn2O6 | 42938 | 1069 | 125,611,0 | 298,15-673 |
| LaKMgMn2O6 | 23711 | 23611 | 6,80,3 | 298,15-673 |
| LaKCaMn2O6 | 39517 | 40,2 | 133,06,0 | 298,15-348 |
|  | 61927 | -(102044) | - | 348-373 |
|  | -(753) | 73331 | 5,80,2 | 373-673 |
| LaKSrMn2O6 | 21118 | 26923 | 141 | 298,15573 |
|  | 1137111 | -(134011) | - | 573-673 |
| LaRbMgMn2O6 | 26712 | 28412 | 362 | 298,15-673 |

Tabulated data show that LaKCaMn2O6 at 348 К and LaKSrMn2O6 at  573 К undergo -type second kind  phase transition.