Calorimetry study of thermal capacity in LaK3Mе3IIMn4O12 (Mе3II – Mg, Ca, Sr, Ba)

Zh.I. Sagintaeva

JSC «Research-and-Production Center «Phytochemistry»

4 Gazaliev str., Karagamda, Kazakhstan, 100009

Е-mail: phytoinform@nursat.kz

Manganites (manganese oxides (III)) of rare earth metals are are of interest due to their magnetic, electric and mechanical properties.

This paper generalizes the results of calorimetry studies which we obtained on the apparatus IT-С-400. The equations of temperature dependencies versus thermal capacities С0рf (Т) for manganites were derived (Table).

| Manganite | Equation coefficient С0р=a+вT+cT-2, J/molК |  |  | Т, К |
| --- | --- | --- | --- | --- |
|  | а | в 10-3 | с 105 |  |
| LaK3Mg3Mn4O12 | 1199 | 125393 | -80,6 | 173-473 |
|  | -7110525 | 8755647 | 8227608 | 47-573 |
|  | -100374 | 2475183 | - | 573-598 |
|  | 24555181 | -3308244 | - | 598-673 |
| LaK3Ca3Mn4O12 | 28517 | 86850 | 211 | 173-373 |
|  | 3856221 | -8750502 | - | 373-423 |
|  | 8443485 | -10808620 | 6651382 | 423-498 |
|  | 89851 | -103960 | - | 498-573 |
|  | 2434140 | -165995 | 3877222 | 573-673 |
| LaK3Sr3Mn4O12 | 18111 | 131883 | 161 | 173-398 |
|  | -7673486 | 10537668 | 6614419 | 398-498 |
|  | 2955187 | -99963 | -5507349 | 498-573 |
|  | 2503159 | -3145199 | - | 573-623 |
|  | -55235 | 1758111 | - | 623-673 |
| LaK3Ba3Mn4O12 | -887 | 2074162 | 181 | 173-398 |
|  | 7759607 | -176721382 | - | 398-423 |
|  | 2949231 | -1376108 | -3727291 | 423-498 |
|  | 6927542 | -12406970 | - | 498-523 |
|  | 1290101 | -22818 | 2003157 | 523-673 |

All manganites have -shaped second kind phase transitions at temperatures: LaK3Mg3Mn4O12 – 473 & 598 К, LaK3Ca3Mn4O12 – 373 & 498 К, LaK3Sr3Mn4O12 – 398 & 598 К, LaK3Ba3Mn4O12 – 398 & 498 К.