Electronic structure and thermodynamic functions of system  Mg - B.

Yu. M. Goryachev, V.I. Dekhteruk, V.Ya. Malakhov, M.I. Siman, L.I. Fiyalka

I.Frantsevych Institute for Problems of Materials Science. Kyiv NASU Ukraine

E - mail: (a) phil02@ukr.net

It is known that magnesium and its connections and in particular borides are extremely perspective in a problem of reduction of weight of vehicles and installations that is very important in global questions of power savings and ecology. However this potential extremely requires the further scientific researches in the field of thermodynamic properties of investigated systems. Authors decide this party of a question on a way of studying of communication of electronic parametres with investigated properties.

The electronic structure of six of the steadiest borides in system – Mg – B is investigated: Mg4B, Mg2B, MgB2, MgB4, MgB6, MgB12. Settlement research has been spent by a method multiclasters a variant (МК) group orbitals a linear combination nuclear orditals (GОLCАО). Parametres of electronic structure of the investigated connections have been defined: an electronic power spectrum, energy of internuclear interaction, density (population) of electronic conditions of a spectrum, charge separate atoms. Data on energy internuclear mutually- actions is resulted in drawing 1. Are  defined it is elastic – and thermodynamic – property and also warmth formation investigated dorides. Some it is given  are resulted in drawing 2 and in the table

Fig. 1. Enthalpy condensation atomic                      Fig. 2. Warmth of formation

dorides magnesium                                            dorides magnesium

. Table.Elastic - dynamic and nuclear - electronic parametres borides magnesium.

|  | А, atomic weight | Z,coordi-nation number | Еат, eV/аtom | d,10-8 сm | ΔFat, eV/atom | β,1010 Pa | Т,mel-ting К | Θ D, Deb,К | TER, 10-6 1/К | Ср, 10-6 eV/аt(K |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mg4B | 21.6 | 11.3 | 2.58 | 2.54 | – 2.56 | 13.6 | 936 | 362 | 6.8 | 8.7 |
| MgB2 | 15.3 | 9.0 | 4.73 | 2.06 | – 4.70 | 37.1 | 1720 | 719 | 4.65 | 2.46 |
| MgB4 | 13.54 | 8.2 | 5.29 | 1.98 | – 5.26 | 42.6 | 1920 | 841 | 4.57 | 1.82 |
| MgB12 | 11.8 | 6.1 | 5.77 | 1.78 | – 5.73 | 47.6 | 2090 | 1050 | 5.63 | 1.2 |

From the finished data exact enough correlation between parametres is visible. The main feature - the big size of hardness in MgB12.