THE EQUATIONS ADSORPTION ACTIVITY AND DIFFERENTIAL ISOSTERIC HEAT OF ADSORPTION

N.A. Makarevich

Institute of Ecological Problems in the North Ural Branch of Russian Academy of Sciences, Arkhangelsk. E-mail: nikma@tut.by (Minsk. Belarus)

For not porous and porous adsorbents (Tab.) the equations of adsorption activity Ga and differential heat of adsorption qst are received . Potentialities of the new equations for definition of thermodynamic characteristics of  adsorption a layer on interfaces a gas, a liquid, a solid are discussed.

The table. The equations isotherms of adsorptions, adsorption activity Ga pure isosteric differential heat of adsorption qst

| Authors of adsorption isotherms | Adsorption isotherms | * Adsorption activity isotherms | * Isotherms of differential isosteric heat of adsorption |
| --- | --- | --- | --- |
| Henry Frandlih Langmur BET Huttig Aranovich Kisarov * Dubinin– Astakhov | (=KHP (=KPn (=KP/(1+KP) (=Сх/[(1-Сх)(1+(С-1)х)] (=Сх(1+х)/(1+Сх) (=Сх/[(1-Сх)(1+х)1/2] ((=Вхn/(1+Вхn) (=Кх1/g/(1+Kх1/g) ((=exp{-{lnx/[(ln(x(=1/e)]}n} | Ga=KH Ga =nKPn-1 Ga =K/(1+KP)2 Ga =C/[1+(C-1)(1-x)2 Ga =C/[1+(C-1)(1-x)2 Ga =(1-2P+KP2)/ [2(1+KP)(1-P)1,5 Ga =nBPn/P(1+BPn)2 Ga =KP1/g / g P(1+KP1/g)2 Ga = -(n/xlnx)· (lnx/ln(x(=1/e)n · {exp[-(lnx/ln(x(=1/e)n] | qst=q0 qst =q0/n qst =q0 qst =q0(1-x)2/ (1-x2+Cx2) qst =q0(1+x)/ (1+2x+Cx2) qst =q0[2(1-x)]/ (2-x+Cx2) qst =q0/n qst =gq0 qst = -q(=1/e (lnx/ln(x(=1/e) |

The note: * - the author; x=P/Ps; (=a/am;  ((= a/a0; K, C, B is const; n is adjust parameter; qst is isosteric of differential heat of adsorption *g=1-(ord+(nord((–1) is the general criterion non-ideality systems, (ord and (nord is thermodynamic probability of an order (association) and the disorder (dissociation) in system, the ( is number of particles to which breaks up (dissociates) a system element; . qo =-RTln[(C((l / (v) + 1+ 1] where (v and (l are according to density in a condition of vaporous and a liquid.