NEW STANDARD DATA ON THERMODYNAMICS OF Pd(aq), O-Pd, Cl-Pd(aq),

O-H-Pd AND O-H-Cl-Pd SYSTEMS

N.A. Polotnyanko

Dubna International University, RF, Dubna, Moscow region, Universitetckaya st., 19,

E-mail: polot.nat@gmail.com

As the result of critical evaluation of the literature data the recommended of thermodynamic values for Pd2+(aq), wich play a key role in the thermodynamic calculations for palladium compounds, has been carried out.

On the basis heat capacity measurements of synthetic crystalline palladium oxide in the temperature range 6.48-328.86 K by the adiabatic vacuum calorimeter [1] and involving literary data on differential scanning calorimetry measurements in the temperature range 370-1065 K [2] the equation of high temperature heat capacity PdO(cr):

Cp (J/mol K) = 3Rn(1 - 0.23∙105T–2) + 4.93∙10–3T (289-1065 К) is obtained.

Using experimental data for PdO(cr) decomposition reaction in the temperatute range 700-1200 K, the recommended thermodynamic values for PdO(cr) Sº(298.15) = 39.58±0.15 J/mol K, ∆fHº(298.15) = -112.69±0.32 kJ/mol and ∆fGº(298.15) = -84.68±0.25 kJ/mol has been carried out. The literature data on solubility Pd(cr), PdO(cr) and Pd(OH)2(аm) in water and water solutions of HClO4 and HCl in wide temperature intervals is considered. The MS-Excel program for “local” consistency procedure of experimental thermodynamic information on chemical systems of interest is used.

This study was supported by Russian Foundation of Basic Research (project 07-05-01108).

LITERATURE

1. Khodakovsky I.L., Smirnova N.N., Bykovа Т.А., Polotnyanko N.A., Kristavchuk A.V., N.D. Shikina, Volchencova V.A., Karimova O.V., Моhov A.V. // Rus. Geochemistry (2009, in press)

2. Nell J., O'Neill H.St.C. // Geochim. Cosmochim. Acta, Vol. 60, N 14, 2487-2493 (1996).