Theoretical Study of Methane Activation on Neutral, Anionic and Cationic Pt4 Clusters with DFT Methods

D.R. Isakov, G.A. Shamov, G.M. Khrapkovskii

Kazan State Technology University, 420015 Kazan, K. Marx str. 68, Russia.

e-mail: isakov@kstu.ru

Gas-phase reactions of sub-nano platinum clusters with small organic molecules often show interesting effects of size and charge of the particle on its reactivity [1]. In this work we present a DFT study on mechanism of methane activation on the Pt4 cluster and its ions. It was shown experimentally that the predominant process there is methane dehydrogenation with formation of methylene-platinum cluster and H2 [1]. We use an all-electron scalar relativistic DFT method in Gaussian basis set with PBE density functional, as implemented in the Priroda code [2]. In our modeling we used, for neutral and ionic Pt4 clusters, tetrahedral structure with triplet and quartet ground states, correspondingly. The first stage of the reaction is formation of a methane-cluster complex. The complex is most stable for the cationic cluster, then for the neutral one, and the least stable for the anion (-18.6, -11.8 and  -7.8 kcal/mol, correspondingly). After that, cleavage of the first C-H bond occur, forming methyl-hydrido-tetra-platinum cluster, and then second C-H bond is cleaved forming methylene-dihydrido-tetraplatinum cluster, which finally loses molecular hydrogen.

For all the Pt4 clusters, cleavage of the first methane C-H bond happens much easier than for the second one. For the cationic cluster, the barrier of the latter stage is the highest, as the TS lies 10.8 kcal/mol higher than separate reagents. At the same time for the neutral and the anionic clusters it lies significantly lower (-4.2 and -10.47 kcal/mol, correspondingly), so that for the former one the breaking of the first C-H bond is the limiting stage. These results allow explaining the experimentally observed inactivity of the Pt4+ cluster towards methane, while Pt4 and Pt4- clusters are very active[1].

References

[1] C. Adlhart, E. Uggerud. Chem. Comm., 24 (2006) 2581-2582.

[2] D.N. Laikov, Chem. Phys. Lett., 461 (2005) 116-120; D.N. Laikov, Chem. Phys. Lett., 281 (1997) 151-156.