Computer models of eutectic type T-x-y diagrams with two inner liquidus fields for two low-temperature modifications of different components

V.I. Lutsyk, V.P. Vorob’eva

Physical Problems Department, Buryat Scientific Center, Siberian Branch of the RAS

670047, Sakhyanovoy str., 8, Ulan-Ude, Russia vvorobjeva@mail.ru

Using the eutectic type T-x-y diagram as an example, it can be represented the analysis of its geometrical construction dependence on the temperature of a component two polymorphous modifications which participate in monovariant metatectic and nonvariant eutectoid (peritectoid) transformations above or below (and within) binary eutectics and below a ternary eutectic. Computer models for considered phase diagrams have been designed. Such models help to solve tasks of visualization, iso- and polythermal sections decoding, mass balances calculation, and definition of monovariant transformation type changing conditions.