UDK 66.021+661.643

E.S.Mustafin.

The Karaganda State University named by E.A.Buketov

Thermal capacity and thermodynamic functions iron and cobalt arsenates

At studying phase balance in systems: As2O5-CoO and As2O5-Fe2O3 [1,2] existence of compounds: Co(AsO3)2, Со2As2O7, Со3(AsО4)2, Со6As2O11, Fe(AsO3)2, Fe4(As2О7)3, FeAsО4, Fe4As2O11 was discovered. Existence of the specified compounds is confirmed by the roentgenophase analysis and T-x phase diagram. For all specified compounds thermal capacities in an interval 298,15-673К by a known technique were determined. Dependence schedules of a thermal capacity from temperature in an interval 298,15-673К are constructed. On the basis of mathematical processing experimental data it has been established, that dependence Cр0-f(T) arsenates J/(mol·К) in an interval 298,15-673К is described by following polynoms.

Table 1.

The equations of temperature dependence of the some arsenates

| Compounds | Equations factors of thermal capacities Ср=а+bТ+сТ-2, J/(mol·К) |  |  | ΔT, К |
| --- | --- | --- | --- | --- |
|  | а | b·10-3 | -с·105 |  |
| 1 | 2 | 3 | 4 | 5 |
| Fе(АsО3)3 | 315±17,7 | 131±7,3 | -104±5 | 298,15-673 |
| Fe4(Аs2О7)3 | 596±32,2 | 411±22,2 | -69±4 | - |
| FeAsО4 | 109±8 | 54±4,3 | 7±0,5 | - |
| Fe4Аs2О11 | 501±3 | 10±0,5 | -108±6 | - |
| Со(AsО3)2 | 285±12 | 29±1,2 | 102±4 | - |
| Со2Аs2О7 | 234±11 | 213±10 | 58±3 | - |
| Cо3(AsО4)2 | 337±17 | 200±10 | 46±2,3 | - |
| Со6Аs2О11 | 513±30 | 25±1,5 | 78±5 | - |

For the first time experimental thermal capacities are by certain for: Со(AsO3)2, Со2As2O7, Со3(AsO4)2, Со6As2O11, Fe(AsO3)3, Fe4(As2O7)3, FeAsO4, Fe4As2O11 in an temperature interval 298,15-673К temperature dependences of thermodynamic functions, such as Cр0(T), S0(T), Фхх(Т), Н0(Т)-Н0(298,15) which can be used at physical and chemical modelling processes of a arsenic conclusion by manufacture of nonferrous metals [1,2] also are calculated.

The literature

1. Kasenov B.K., Mustafin E.S. The balance phase in system As205-СоО//Inorganic chemistry magazine. – 1996. Т. 41.№9. p. 19761-1977.

2. Kasenov B.K., Mustafin E.S. The balance phase in system As205-Fe20з// Inorganic chemistry magazine. – 1997. Т. 42.№10. p. 1746-1747.